# On line Structural Health Monitoring of Composites using Screen Printed Nano-Composite Sensors

Taimoor A. Khan, Department of Aeronautics & Astronautics, Institute of Space Technology, Islamabad, Pakistan

Saad Nauman, Department of Materials Science & Engineering, Institute of Space Technology, Islamabad, Pakistan

Zaffar M. Khan, Department of Aeronautics & Astronautics, Institute of Space Technology, Islamabad, Pakistan

### Abstract

This research aims to develop CNPs based piezoresistive sensor through screen printing and correlate the strain rate to predict the failure response of glass fibre composites. This involves homogenous dispersal of carbon nano- particles (CNPs) in polystyrene (PS) resin through sonication. The smart sensing layer is deposited on glass fibre reinforced composite structures for sensing. The concentration of CNPs was maintained at the percolation threshold of 35% by weight which ensured higher sensitivities and damage detection capability. The composite notched specimens were tested in tension according to ASTM standard to validate the sensing characteristics of the smart layer.

### It was found that the screen printed smart sensing layers were capable of monitoring strains like traditional strain gauges but with higher gauge factors of 20. The screen printing techniques, due to its low cost and easy implementation, is recommended as a reliable method of sensor integration on various types of substrates including plastics & composites

### Image

### Fig 5. a) Screen, b) Schematic of screen printing process

Recent Publications

- Rahim Jan, Amir Habib, Zaffar M Khan, Muhammad Bilal Khan, Muhammad Anas, Ali Nasir and Saad Nauman (2016): Liquid exfoliated graphene smart layer for structural health monitoring of composites.

- Zaffar M. Khan, M.B. Khan, M. Bassyouni, S.M.-S. Abdel-Hamid, M.H. Abdel-Aziz, Syued W. ul Hasan (2016): Fabrication and Thermomechanical Characterization of Glass Fiber/ Vinyl Ester Wind Turbine Rotor Blade.

- Zaffar. M. Khan, D.O. Adams and S. Anis (2016): The Influence of Multiple Nested Layer Waviness on the Compression Strength of Double Nested Wave Formation in Carbon Fiber Composite Laminate

- M. A. Nasir, Zaffar M. Khan, Ilyas Farooqi, Saad Nauman, Shahid Khalil, Asim Pasha, Zubair Khan, H. Qaiser (2015): Transverse Shear Behavior of Nomax Core for Sandwich Panel.

- Laraib Alam Khan, Ali Hasan Mahmood, Bilal Hassan, Tahir Sharif, Shahaab Khushnod, Zaffar M. Khan (2014): Cost-effective manufacturing process for the development of automotive from energy efficient composite materials and sandwich structures

Biography

Taimoor Ahmad Khan was born in Khan Garh, Pakistan in 5Aug, 1991. He received Pre- engineering degree form G.C.U (Government college university), Lahore Pakistan and B.E degree in Materials Science from NUST (National University of Sciences and Technology), Islamabad Pakistan, in 2008 and 2012 respectively. In 2014 he got admission in Master Program in Aerospace engineering (Structural Design & Analysis) in IST (Institute of Space Technology) Islamabad where he is still working as a master student.

Email: taimoor.khan95@gmail.com