Correlation between densification and ferromagnetic resonance of Rare-Earth substituted magnetic oxides
Alina Manzoor1,2, Muhammad Azhar Khan 1, Wolfgang Kuch3

1Department of Physics, The Islamia University of Bahawalpur, Bahawalpur-63100, Pakistan.

2Department of Physics, Government College University, 38000 Faisalabad, Pakistan.

3Institut für Experimental physik, Freie Universität Berlin, 14195 Berlin, Germany.

Email: aleena.qau@gmail.com, +923328665304

Abstract

In the present study, we report the dopant- and size-dependent variations in high-frequency magnetic and electrical transport properties of Ho-substituted Li-Mn polycrystalline ferrites. Thermal stability and phase identification were confirmed by thermal gravimetric analysis and X-ray diffraction experiments. The overall average crystallite size decreased from 29.6 to 17.5 nm, whereas the bulk density increased from 3.47 to 4.29 g/cm3 with increasing Ho content. Ferromagnetic resonance (FMR) measurements at the X-band revealed significant shifts in FMR linewidths and resonance positions as a function of composition. Both, FMR linewidth and porosity, were found to decrease with the systematic addition of Ho from 2538 to 2359 Oe and from 26 to 15.4 %, respectively. The substitution of Ho3+ for Fe3+ reduced the net magnetization of the spinel lattice from 53 to 41 emu/g. Electrical measurements revealed that the resistivity is higher in samples with smaller grains possessing a greater number of thin insulating grain boundaries. The activation energy ∆E required for hopping increases from 0.09 to 0.16 eV with Ho addition, which may be well explained by the increase in resistivity. The substitution of Ho3+ for Fe3+ causes a decrease in Curie temperature Tc due to the damping of A-B exchange interactions.

Keywords: Magnetic materials, Exchange interactions, Ferromagnetic resonance, Electrical resistivity

Recent Publications:

- Zaheer Ahmad, Amir Muhammad Afzal, Muhammad Farooq Khan, Alina Manzoor, Hafiz M. W. Khalil, and Sikandar Aftab, Copper-Doped Nickel-Oxide Nanoparticles for Photocatalytic Degradation of Erichrome Black-T and Methylene Blue and its Solar Cell Applications, Journal of Nanoelectronics and Optoelectronics (Accepted)

- A. M. Afzal, Alina Manzoor, Muhammad Zubair Khan, M. F. Khan, Aftab Skindar, Umair Anwer and Zaheer Ahmad, Effect of Cobalt Substitution on Magnetic, Resistivity and Dielectric Properties of Nickel-Zinc Ferrite (CoxNix-0.5Zn0.5Fe2O4), Journal of Nanoelectronics and Optoelectronics (Accepted)

- M. Nasir Rasool, Altaf Hussain, Asifa Anam, M. Atif Sattar, Alina Manzoor, DFT based structural, electronic and optical properties of B_(1-x) In_x P (x= 0.0,0.25,0.5,0.75,1.0) compounds: PBE-GGA vs. mBJ-approaches, Chinese Journal of Physics, 56 (2018) 2659-2672

- Alina Manzoor, Muhammad Azhar Khan, Muhammad Yaqoob Khan, Majid Niaz Akhtar, Altaf Hussain, Tuning magnetic and high frequency dielectric behavior in Li-Zn ferrites by Ho doping, Ceramics International 44 (2018) 6321–6329

- Muhammad Irshad, Muhammad Azhar Khan, Sajjad Ahmad Khan, Irshad Ali, Ghulam Murtaza, Muhammad Naeem Ashiq, Abdul Aziz, Alina Manzoor, Improved electrical, magnetic and dielectric properties of polypyrol (PPy) substituted spinel ferrite composites, Physica E 93 (2017) 313–317.

Biography:

I am Alina Manzoor, working as Assistant Professor at Government College University Faisalabad, Pakistan. I have done my PhD in the field of nanomagnetism from The Islamia University of Bahawalpur, Pakistan. I have thirteen international publications from my research work in various international journals. I have just completed a research project as a guest researcher at Freie University Berlin, Germany with AG KUCH group in the department of experimental physics.

Full name: Alina Manzoor

University/Industry/Organization name: Government College University Faisalabad

Designation:  Assistant Professor

Country: Pakistan

Mobile number: +923328665304

Email: aleena.qau@gmail.com

Track number: https://condensedmatterphysics.euroscicon.com/abstract-submission (For track number follow this link
Category: Poster presentation

Research interest: Nano-structured magnetic materials, thin films, hetrostructures, multiferroics, composites, etc

Date of birth: 20-12-1985