Comparison of the effects of anti-stripping fillers and nanomaterials on moisture resistance of asphalt mixes

Amir Kavussia,*, Seyed-Hamed Razavia

a Faculty of Civil and Environmental Engineering, Tarbiat Modares University, Tehran, Iran

ABSTRACT

The role of some active fillers in increasing moisture resistance of asphalt mixes has been proved since few decades back. Nanomaterials have recently been used to modify bitumen binders and enhance properties of asphalt mixes. The aim of this research was to compare the effects of active fillers (such as hydrated lime), and these in their nano size conditions.

In order to produce nano-hydrated lime in laboratory, a planetary rotary ball mill was used and nano-hydrated lime was produced from hydrated lime filler. In addition, calcium carbonate filler and a nano-calcium carbonate material were selected too. The particle size distribution of produced nano-hydrated lime was determined using Scanning Electron Microscope (SEM) and Dynamic Light Scattering (DLS) techniques. With applying these methods, it was possible to determine the approximate sizes of the tested nanomaterials, although some differences were observed in the two methods. For the produced nano-hydrated lime, sizes of 125 and 208 nm were recorded, respectively in these methods. In this study, nano-hydrated lime, nano-calcium carbonate, nano-bentonite and nano-silica, and two types of antistripping fillers, namely hydrated lime and calcium carbonate as additives were selected.

Each of the above additives was mixed with a 60-70 pen bitumen at different concentrations, using a conventional mixer. With using FE-SEM testing machine, it was assured of the good distribution and homogeneity of all the filler-bitumen and nanomaterial-bitumen blends.

A hard and siliceous aggregate type was selected and the above blends were used to prepare compacted bituminous samples. Indirect Tensile Stiffness Modulus (ITSM) testing was performed and a parameter named “Index of Retained Resilient Modulus (IRMr)” was determined for comparison purposes and for ranking the various mixes. The findings of the research indicated that when nanomaterials were used, a lower rate of material (compared with the same material in its filler size) would be needed in the mix so that to produce similar effects in terms of resistance against moisture damage. For hydrated lime, for example, 4% nano-hydrated lime provided similar effects on mixes that 20% hydrated lime filler had.

Keywords: Nanomaterials, Mineral fillers, Moisture resistance, Resilient modulus

*Corresponding author. Tel.: +98 21 8288 3331.

E-mail addresses: kavussia@modares.ac.ir (A.Kavussi), h.razavi@modares.ac.ir; se.hamed.razavi@gmail.com (S.H. Razavi).

Biography Amir Kavussi has completed his PhD at the age of 28 from University of Birmingham in UK. He has been working in Tarbiat Modares University (TMU) as a lecturer since 1990. He is presently the head of highway group in TMU. He has published numerous journals papers in reputed journals and has been serving as an editorial board member of several journals. His research works are focused on properties of bituminous materials. Numerous master and PhD students were graduated under his supervision. Currently he is a technical committee member in MESAT (Middle East Society of Asphalt Technologists). He is also research deputy of Pavement Management Centre of TMU.