Investigation of NH3 Gas Sensing Behavior of Intercalated PPy – GO – WO3 Hybrid Nanocomposite at Room Temperature

Heiner A J, Gurunathan K*

Nano Functional Materials Lab, Dept. of Nanoscience & Technology, Alagappa University, Karaikudi – 630 003, Tamil Nadu, India.

Polypyrrole, Graphene oxide and WO3 nanostructures are synthesized by chemical polymerization, Modified Hummers method and hydrothermal method respectively. PPy – GO – WO3 hybrid nanocomposite is synthesized by the polymerization of polypyrrole in the presence of GO – WO3 nanocomposite. Surface morphology is analyzed using SEM and HRTEM. Crystalline nature and chemical composition of the sensing materials are examined by X-ray Diffraction Spectroscopy and Fourier Transform Infrared Spectroscopy respectively. Band gap energy of the hybrid nanocomposite is calculated as 4.1 eV using UV –Visible absorption spectroscopy. Electrodes are fabricated by spin coating the sensing materials on a Printed Circuit Board. The electrodes have been investigated for their response towards Oxygen, Hydrogen, Ammonia and Liquid Petroleum Gas at room temperature. Among the different gases, electrodes are selectively sensitive to ammonia gas with improved sensitivity (58 %), response time (50 Sec) and recovery time (120 Sec) in the presence of 10 ppm gas. The lower limit of detection of the electrode is observed as 5 ppm. The reproducibility of the response of the electrodes is tested and it is stable for the period of 50 days.

Key Words: Polypyrrole, Graphene Oxide, Tungsten Oxide, Hybrid Nanocomposite, Ammonia

Authors Biographies

Heiner Albaris received his BE Electronics and Communication degree from Anna University Chennai in 2013. He has been received his M.Tech Nanoscience and Technology degree from Anna University, Chennai in 2015. Currently he is pursuing Ph.D., under the supervision of Prof. Gurunathan Karuppasamy in the department of Nanoscience and Technology, Alagappa University, Karaikudi. His areas of interest are Nano electronics, Nano Gas Sensors based on conducting polymer.

Gurunathan Karuppasamy received his Bachelor and Master of Science in Chemistry from Madurai Kamaraj University. He pursued Ph.D Chemistry – Energy from Madras University, Chennai. He visited many countries with prestigious fellowships like BOYSCAST Fellow (USA) and Brain Pool Scientist (South Korea). He worked as Research Associate in CSIR - Central Electrochemical Research Institute, Karaikudi, India. Then He moved to Centre for Materials for Electronics Technology, Pune, India as Scientist. Currently he is working as Professor and Head in the department of Nanoscience and Technology, Alagappa University, Karaikudi, India. His research area covers Photocatalysis, Hydrogen production and storage, Solar cell, Nano electronics and conducting polymer based energy devices and gas sensors.

Presenting author details 
Full name: Heiner Albaris
Contact number: +91 94893 93913
Twitter account: AjHeiner
Linked In account: arnoldajheiner@gmail.com

Session name/ number:
Category: Poster Presentation