Title: Improve microstructure and mechanical properties of Cf/SiC- Cf/SiC joint by TiCoNb + Nb foil

Name: Qiang Zhang, Jie Zhang

School of Materials Science and Engineering, Harbin Institute of Technology,

Harbin 150001, PR China

Ti35Co35Nb30 eutectic filler alloy was used to braze Cf/SiC composite. The results showed that there were many large TiCo intermetallic compounds in the brazing seam, and the shear strength of the joint was only 34.4MPa. To improve the microstructure and mechanical properties of the joint, Nb foil was introduced into the filler alloy. Nb can melt into the liquid solder to adjust liquid solder composition during brazing process. The effect of holding time on the microstructure and mechanical properties of brazed joints was investigated. With extending the holding time, the Nb foil thinning and disappeared gradually, TiCo and Nb(s,s) eutectic and CoNb4Si compound increased, and massive TiCo intermetallic compounds disappeared. The highest shear strength with 66 MPa was received while the joint brazed at 1300°C for 15min.

Biography

Qiang Zhang, a Ph.D candidate at Harbin institute of technology. He has published 2 academic papers in Journal of the European ceramic society and Materials Science and Engineering: A, and was granted 2 patents.

Presenting author details 
Full name: Qiang Zhang
Contact number: +86 18945054207
Twitter account:
Linked In account:

Session name/ number: Ceramic Materials/ Track 2-6
Category: Poster presentation