Title: Design of filler metal based on finite element simulation

Name: Jie Zhang, Qiang Zhang

School of Materials Science and Engineering, Harbin Institute of Technology,

Harbin 150001, PR China

Residual stress has great influence on the mechanical properties of the joints. Finite element analysis software was used to simulate the residual stress of the Cf/SiC-Nb joint after cooling. The effect of yield strength, thermal expansion coefficient and elastic modulus of the filler alloy on the residual stress of the Cf/SiC-Nb joint was investigated. The results showed that the lower the yield strength and thermal expansion coefficient was, the smaller the residual stress of the joint was. A novel Ti35Co35Nb30 (at.%) high temperature filler alloy was designed based on the finite element simulation results, and the microstructure and thermal physical properties of the filler alloy were investigated. The Cf/SiC-Nb joint brazed with this filler alloy exhibited high shear strength up to 178MPa, which is mainly attributed to the satisfactory brazing seam microstructure with good thermal and physical properties.

Biography

Jie Zhang, PhD, Professor, director of analysis and measurement center of Harbin institute of technology. She has conducted the national natural science fund project, national defense pre-research project, provincial projects, and a number of international cooperation projects, etc. She has won a national natural science award (third class), a Ministry of Education science and technology progress award (first class), a Heilongjiang province natural science award (second class), an aerospace science and technology progress award (third class). She has published more than 80 academic papers and was granted 8 patents.

Presenting author details 
Full name: Jie Zhang
Contact number: +86 0451-86414234
Twitter account:
Linked In account:

Session name/ number: Ceramic Materials/ Track 2-6
Category: Poster presentation