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Abstract
Rare-Earth Transition Metals permanent magnets are vital components in the rapidly-developing renewable energy sector, where the motors for electric vehicles and the generators in wind turbines require strong magnets with the ability to operate at temperatures well over 100°C. To achieve high coercivity, remanence and consequently high-energy product at elevated temperatures the addition of heavy rare earth (HRE) to the basic Nd-Fe-B composition is needed. On the list of Critical Raw Materials published by the EC in 2014, HRE is on the very top of it. To drastically reduce the use of HRE we focused on developing a new method, which should enable us to achieve the properties needed for high-temperature application with the lowest amount of scarce elements.  
The significant progress was attained by using electrophoretic deposition as a method for accurately positioning the HRE on the surface of a sintered Nd-Fe-B magnet before its diffusion into the microstructure. After the additional annealing, this process locally increased the coercivity of final magnet, thereby substantially reducing the dependence on the HREs, Dy, and Tb1-3. By our new inventive technique further transferred to a pilot production, we could minimize the amount of HRE used, down to 0.2 at %, the improvement of coercivity was 30 % with minimal loss in remanence. The total saving of the HRE is 16-times less need for the same performance, which is a significant contribution to the world economy and clean environment. 
In studying the mechanism for such an improvement in coercivity without significantly decreasing the remanence, a detailed microstructure investigation was performed by using high-resolution transmission microscopy and analysis at the nano level (Fig. 1).  
Besides the use of these new developed high energy magnets for electric and hybrid cars and the wind turbine generators the important application is also as the source of the magnetic field in the development of the new magnetic cooling devices. 
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Recent PublicationsFig. 1. Electron Holography of the core/shell region. (a) Total phase image with marked location of the grain boundaries (GB) and the triple pocket (TP). (b) Reconstructed phase showing the magnetic flux distribution and color maps. The contour spacing is π/2.
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