Performant cement based materials reinforced with nano-SiO2
Mihaela-Andreea Moncea, Florina-Diana Dumitru, Marius Viorel Olteanu, Madalina Boboc, György Deák

National Institute for Research and Development in Environmental Protection, 294 Splaiul Independentei, 6th District, 060031, Bucharest, ROMANIA

The paper presents the investigation of the effect of SiO2 nano-particles on the mechanical properties and microstructure of cement based materials. For this purpose nano-SiO2 powders were obtained by sol-gel method using different molar ratios of TEOS/ethanol/water. The formation of nano-SiO2 particles was confirmed by X-ray fluorescence analyses (XRF) and the nanometric sizes by scanning electron microscopy (SEM).

The cement based materials admixture were obtained by using 0.45 and 0.5 water/binder ratio (w/b) and for each ratio the cement was substituted with 0.5 respectively 0.7 % of nano-SiO2. The distribution of nano-SiO2 particles within the cement matrix plays an essential role and governs the performance of these products. Therefore, the addition of 0.4% superplasticizer for the w/b = 0.45 was proposed to facilitate the distribution of nano-SiO2 particles. The mechanical test results showed that after 7 days of hydration the cement based materials with 0.7% nano-SiO2 content improved the compressive strengths compared with those of the etalon (E=45MPa vs. AM1=55MPa). The microstructure of cement based admixtures highlighted the presence of Ca(OH)2, ettringite and calcium silicate hydrates as well as nano-SiO2 particles embedded into the cement matrix.

Biography

Mihaela-Andreea Moncea has completed his PhD at the age of 30 years from Politehnica University of Bucharest. She is senior researcher at the National Institute for Research and Development in Environmental Protection, within the Impact of Built Environment and Nanomaterials Department. She has published more than 30 papers and is serving as reviewer at an ISI specialised journal in the materials science field.

Presenting author details 
Full name: Mihaela-Andreea MONCEA
Contact number: +40 (0)21 305 26 72
Twitter account:-
Linked In account:-

Session name/ number: Nanoparticle Synthesis and Aplications
Category: Poster presentation