Fabrication of high-quality magneto-optical TAG transparent ceramics

Shengming Zhou, Shanghai Institute of Optics and Fine Mechanics, CAS, Shanghai , China.

Abstract (300 word limit)

Terbium aluminum garnet Tb3Al5O12 (TAG) single crystal is an excellent magneto-optical material with good transmittance in the 500-1500nm region, high thermal conductivity, and higher Verdet constant than the most commonly used terbium gallium garnet Tb3Ga5O12 (TGG) single crystal. However, it is extremely difficult to grow TAG single crystal from the melt because of its incongruent melting nature. TAG transparent ceramics not only remain the excellent magneto-optical property of TAG crystal, but also can realize large size growth. In this work, high-quality (Tb1-xRx)3Al5O12 (R=Ce, Si, Ti) transparent ceramics were synthesized by solid state reaction and vacuum sintering. Effect of additions on TAG transparent ceramic was characterized. The Verdet constant of the Ce3+ doped TAG transparent ceramic measured at 632.8nm was -199.55 rad.T-1.m-1, which was larger than that of the pure TAG transparent ceramic (-172.8 rad.T-1.m-1) , Si:TAG (-173.4 rad.T-1.m-1) and Ti:TAG (-184.2 rad.T-1.m-1). The Ti-doping has an obvious effect on controlling average grain size, homogenizing grain size, and eliminating pores, and therefore Ti:TAG has the highest transmittance (81% in the region of 550nm-1500nm). It is obtained that the Verdet constant of all doped TAG samples is ∼40% higher than that of TGG ceramics at 1064 nm. Especially, Si:TAG has magnetooptical figures of merit more than 1.5 times greater than those of TGG ceramics. The mechanism of these observed phenomena is proposed in this presentation and it is suggested that Si:TAG is a promising for the application of high-power Faraday isolators.

Image

High-quality magneto-optical TAG transparent ceramic fabricated by Shanghai Institute of Optics and Fine Mechanics

Recent Publications (minimum 5)

- Aleksey Starobor, Oleg Palashov, and Shengming Zhou (2016) Thermo-optical properties of terbium-aluminum garnet ceramics doped with silicon and titanium. Opt. Lett. 41:1510-1513.

- Hiroaki Furuse, Ryo Yasuhara, Keijiro Hiraga, and Shengming Zhou (2016) High Verdet constant of Ti-doped terbium aluminum garnet (TAG) ceramics. OPTICAL MATERIALS EXPRESS 6:191-196.

- Chong Chen, Xuezhuan Yi, Shuai  Zhang, Yue Feng, Yanru Tang, Hui Lin, Shengming Zhou (2015) Vacuum sintering of Tb3Al5O12 transparent  ceramics with combined TEOS+MgO sintering aids. Ceramics International 41:12823–12827.

- Dmitry Zheleznov, Aleksey Starobor, Oleg Palashov, Hui Lin and Shengming Zhou (2014)  Improving characteristics of Faraday isolators based on TAG ceramics by cerium doping. OPTICS LETTERS 39: 2183-2186.

5. Dmitry Zheleznov, Aleksey Starobor, Oleg Palashov, Chong Chen, and Shengming Zhou (2014) High-power Faraday isolators based on TAG ceramics. OPTICS EXPRESS  22: 2578-2583.

Prof. Dr. Shengming Zhou

Key laboratory of Materials for High Power Laser,

Shanghai Institute of Optics and Fine Mechanics,

Chinese Academy of Sciences, Shanghai, China

Email: zhousm@siom.ac.cn

Notes/Comments: