11th International Conference on Advanced Materials & Processing

Edinburgh, Scotland

September 6&7 2017

Evaluation of hydrocarbon based Non fluorinated Membranes as electrolytes for efficient Microbial Fuel Cell performance

Dharmalingam Sangeetha

Department of Mechanical Engineering, Anna University, Chennai -600 025, India

Corresponding Author Email: sangeetha@annauniv.edu Tel: +912235 7763

Abstract:

Microbial Fuel Cell (MFC) is a bio-electrochemical method that drives a current via bacteria and mimicking bacterial interactions found in nature. Proton exchange membrane is one of the essential components of membrane based microbial fuel cells (MFCs).The generally used membrane available commercially is Nafion. Nafion has several limitations including high cost, substrate crossover, oxygen leakage and accumulation. Hence, intensive research is carried out to find a suitable membrane to overcome the problems of oxygen cross over and substrate loss. The alternate membrane should be environment friendly, with increased power density and should be cost effective than the fluorinated Nafion membrane in addition to lower oxygen permeability to maintain an anaerobic environment in the anodic chamber of the cell. Our research focuses on non fluorinated polymer membranes such as Sulfonated Poly Ether Ether Ketone (SPEEK), Sulfonated Poly Styrene Ethylene Butylene Poly Styrene (SPSEBS), Quaternized Poly Ether Ether Ketone (QPEEK), Quaternized Poly Sulphone (QPSU), Quaternized Poly Ether Imide (QPEI) and chitosan and their composites. The physico-chemical properties of the composite membranes such as water uptake, ion–exchange capacity, ionic conductivity, dissolved oxygen cross over, durability and transport of cations were studied for the suitability in MFC. The presentation will highlight the performance of such lab synthesized membranes in a Microbial Fuel Cell lab made set up in terms of maximum power density and efficiency.

| S.No | Membrane | Max. Power Density (mWm-2) | Features | References |
| --- | --- | --- | --- | --- |
| 1 | SPEEK | 570 | Single Chamber Microbial Fuel Cell (SCMFC), Escherichia coli, Cation exchange membrane (CEM) | Sivasankaran et al; Bio Resource Technology (2011) |
| 2 | SPSEBS | 590 | SCMFC and Dual Chamber MFC (DCMFC), Mixed culture, CEM | Sivasankaran et al; Journal of Power Resources (2012) |
| 3 | SPEEK-Suplonated SiO2 | 1008 | SCMFC, Mixed culture, CEM | Sivasankaran et al; Fuel (2015) |
| 4 | SPSEBS- Suplonated SiO2 | 1209 | SCMFC, Biocatalyst – Mixed culture, CEM | Sivasankaran et al; Chemical Engineering Journal (2016) |
| 5 | SPSEBS-Suplonated TiO2 | 1345 | SCMFC, Mixed culture, CEM | Sivasankaran et al; Energy (2015) |
| 6 | SPEEK- Suplonated TiO2 | 1202 | SCMFC, Mixed culture, CEM | Sivasankaran et al; RSC Advances (2013) |
| 7 | QPSU-FGO | 1036 | SCMFC, Mixed culture, Anionic exchange membrane (AEM) | Mahendravarman et al; RSC Advances (2016) |
| 8 | QPEI | 612 | SCMFC and DCMFC, Mixed culture, AEM | Mahendravarman et al; International Journal of Hydrogen Energy (2016) |
| 9 | QPEEK | 600 | SCMFC, Mixed culture, AEM | Mahendravarman et al; International Journal of Hydrogen Energy (2013) |
| 10 | MWCNT-chitosan | 41 | SCMFC, Mixed Culture, Chitosan as a biocompatable membrane | Prabhu et al; Journal of Membrane Science (2013) |