Meso Porous Hybrid Silica Gel Frameworks for Low Temperature CO2 Adsorption

Minju Ashok, A. Peer Mohamed, S. Ananthakumar, and S. Savithri*

Materials Science and Technology Division

Council of Scientific and Industrial research- National Institute for Interdisciplinary Science Technology Division Thiruvananthapuram, Kerala, INDIA

### Abstract (300 word limit)

Meso porous inorganic silica gel supports have been processed via sol-gel technique from economically affordable water-glass precursors. An injectable gel was prepared first from water-glass which was then transformed into solid silica gel spheres through self-assembly route. Subsequently, the gel supports were chemically activated with various amine functional groups to develop gel-sorbents for CO2 adsorption. The thermal stability, morphology, surface area and porosity features were assessed and correlated with the CO2 adsorption efficiency.

Amine activated gel porous adsorbents showed working capacity as CO2 adsorbent at temperatures as low as 100oC, appears to be promising for CO2 sorption in flue gas stream. CO2 adsorption isotherms indicate the gel-sorbents activated with APTMS offered higher adsorption performance at 75 oC.  The sorbents prepared with the mixture of APTMS and TEPA offered a CO2 adsorption capacity of 3.26 mmol g-1 at 75 oC. Inorganic hybrid gels combined with the appropriate pore engineering and chemical activation using multiple-amines permit effective accessibility for the CO2 gas and its adsorption that ultimately result in enhanced adsorption at low operating temperatures.

### Recent Publications (minimum 5)

- N. Minju, P. Abhilash, Balagopal N. Nair, A. Peer Mohamed, S. Ananthakumar, (2015),  Amine impregnated porous silica gel sorbents synthesized from water–glass precursors for CO2 capturing. Chemical Engineering Journal, 269,335-342.

- O.A. Esam, CO2 capture on porous adsorbents containing surface amino groups, Electronic Theses and Dissertations (2013) Paper 2304.,

- A.K. Mishra, S. Ramaprabhu,  Polyaniline/multiwalled carbon nanotubes nanocomposite – an excellent reversible CO2 capture candidate, RSC Adv. 2 (2012) 1746–1750.

- A. Samanta, A. Zhao, G.K.H. Shimizu, P. Sarkar, R. Gupta, Post-combustion CO2 capture using solid sorbents: a review, Ind. Eng. Chem. Res. 51 (2012) 1438– 1463.

Biography

Dr. S. Savithri  is working as a senior principal scientist in Computational Modeling and Simulation Section at the National Institute for Interdisciplinary Science & Technology which comes under Council of Scientific and Industrial Research(CSIR-NIIST)  since 1992.  She started her career in mathematical modelling and simulation area with a graduation and post graduation in Applied Mathematics from Maduari kamaraj University. She obtained her Ph.D. in 1992 from IIT, Madras. Her field of interests are

- Mathematical modelling of Solidification & Casting Process

- Technical software development

- CFD simulation of  multiphase flows

- Discrete element simulation of granular flows

Email: sivakumarsavi@gmail.com

Notes/Comments: