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Abstract
In the present work, a failed connecting rod from a motorcycle engine was investigated for the root cause of and possible mechanisms leading to its premature failure.  In addition to finding the root cause, the expectation from this study was to possibly improve the existing designs or practices to avoid similar failures in future. These results were validated using a finite element analysis (FEA) simulation. A Scanning Electron Microscope was used for investigating the mechanisms of fracture modes, optical microscopy for studying the microstructures and visual inspection were primarily utilised to determine the root cause of the failure. In conclusion, it was determined that the root cause for the premature failure of the connecting rod was the presence of scale build-up inclusions, which led to micro cracking during fatigue loading of the component.
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Figure 1:(a) Diagram of an assembled connecting rod, rod cap, bolts and slip bearing with key features and components annotated in red; (b) The intact and failed connecting rod and piston assemblies, left and right consecutively, are shown with the failure.
· It is most likely that the connecting rod failed on the end of exhaust stroke, due to the tensile force being at its highest, when the piston reaches TDC. This is due to the inertia of the piston, pin, and upper end of the connection rod moving upwards while there are no compressive forces to take them under consideration.
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