# Development of high-order multicomponent Al-Cu based eutectic alloys

Isaac TH Chang, BCAST Brunel University London, UK.

### Abstract

Eutectic alloys have a lower melting point and excellent castability. Their composite microstructure exhibits excellent mechanical properties. Recently, near eutectic Al-Cu-Si ternary alloys has received increasing attention due to a combination of ultrahigh compressive strength (1GPa) and good plasticity (11%), which are attributed to the nano/ultrafine structure composites containing either micron-sized dendrites embedded in ultrafine eutectic matrix or multi-scale eutectic microstructure.

This paper presents a study of the lamellar eutectic microstructure in higher-order multicomponent (Al-Cu-Si, Al-Cu-Si-Mg, and Al-Cu-Si-Mg-Zn) systems, as compared to its binary Al-Cu counterpart. Eutectic alloys of binary Al-Cu, ternary Al-Cu-Si, quaternary Al-Cu-Si-Mg and quinary Al-Cu-Si-Mg-Zn systems were prepared using arc melting and suction casting processes. These samples were then characterized using a combination of X-ray diffraction, scanning electron microscope and Vickers hardness test. All as-cast alloys consisted of a lamellar eutectic microstructure. It was found that the average interlamellar spacing reduced significantly from 84±8 nm to 41±4 nm, with increasing number of principal alloying elements from binary Al-Cu to quaternary Al-Cu-Si-Mg eutectic systems, respectively. This led to an increase in average Vickers hardness value from 280 in binary Al-Cu to 339 in quaternary Al-Cu-Si-Mg alloy. The presentation will discuss the effect of increasing number of principal alloying elements on the eutectic microstructure and its mechanical property. The current results open up new opportunities to design a novel ultrafine eutectic microstructure in the high-order multicomponent alloys with potentially superior mechanical properties.

Recent Publications (minimum 5)

- Sanderson P, Su SS, Chang, ITH, Delgado Saborit JM, Kepaptsoglou DM, Weber RJM, Harrison RM (2016) Characterisation of iron-rich atmospheric submicrometre particles in the roadside environment. Atmospheric Environment 140:167-175

- Peng T, Chang ITH (2015) Uniformly Dispersion of Carbon Nanotube in Aluminum Powders by Wet Shake-mixing Approach.  Powder Technology  284: 32-39.

- Peng T, Chang ITH (2014) Mechanical alloying of multi-walled carbon nanotubes reinforced aluminum composite powder. Powder Technology 266: 7-15.

- Su S, Chang ITH, Lead J, Pikramenou Z, Kuo WCH (2014) Production of Zinc Oxide using Pulsed Electrical Discharge in Liquid. Journal of Nanoparticle Research 16 (9):2611-2623.

- Su S, Chang ITH (2013) Effects of Processing Conditions on the Sintering Response of Hypereutectic Al-Si-Cu-Mg P/M Alloys. Materials Chemistry and Physics 139: 775-782.

Biography (150 word limit)

Isaac Chang was appointed as a Professor of Metallurgy & Materials at Brunel Centre for Advanced Solidification Technology (BCAST), Brunel University London in 2016. Prior to this, he was a Reader at School of Metallurgy and Materials, University of Birmingham. He received his DPhil in Materials Science from University of Oxford and BSc(Eng) in Materials & Metallurgy from Imperial College, London University. He specializes in the field of physical and powder metallurgy, as well as nanotechnology and ceramic science. His research is focused on the understanding of the relationship between composition, processing, microstructure and properties of various materials, including high entropy alloys, aluminium alloys, metallic glasses, nanoparticles and superhard ceramics for industrial applications in transport, energy, healthcare, defence and electronic sectors. He is a Fellow of UK Institute of Materials, Minerals and Mining (IOM3) and a member of the editorial board for Journal of Materials, Chemistry and Physics.

Email: isaac.chang@brunel.ac.uk

Notes/Comments: