Natural plant-derived polymer fabricated with sugar-containing hydroxyapatite for biocompatible bone-hemostasis

Y. NOH*1, T. Umeda1, T. Musha2, T. Sasaki3 and K. Itatani1

1Department of Materials and Life Sciences, Sophia University, 7-1, Kioi-cho, Chiyoda-ku, Tokyo 102-8554, Japan; 2Department of Orthopaedic Surgery, Toho University, 2-17-6 Ohashi, Meguro-ku, Tokyo 153-8515, Japan; 3Research Institute of Electronics, Shizuoka University, 3-5-1 Johoku, Naka-Ku, Hamamatsu 432-8011, Japan.

Abstract

The preparation conditions of bone-hemostasis materials were examined using hydroxyapatite (Ca10(PO4)6(OH)2: HAp) and natural plant-derived polymer(guar gum(GG), locust bean gum(LBG) and sodium alginate(AG)). The starting gel was prepared by dissolving 2 mass% 80LBG-20GG and 2 mass% AG into deionized water heated at 60ºC (80LBG-20GG/AG). The resulting gels were vigorously agitated with 20,000 rpm for 3 min. Further, the gel was immersed into 3 mass% phosporyl oligosaccharides of calcium (POs-Ca®50) solution at room temperature for 24 h. Then, the resulting gel was hydrothermally-treated 100ºC for 5 h and freeze-dried at -50ºC for 24 h to form s-HAp in the material.

According to the X-ray diffractometry (XRD), Fourier transform infrared spectrometry (FT-IR) and confirmed by the terahertz spectroscopy, the resulting composite contained hydrolyzed materials of POs-Ca, i.e., the sugar-containing HAp (s-HAp), as well as LBG and GG. According to the micro-computed tomography (micro-CT) and differential thermal analysis and thermogravimetry (DTA-TG), 16.8% of HAp could be homogeneously dispersed within the porous composite material. The pore sizes were approximately 1 to 2 µm determined by scanning electron microscopy (SEM).

The present 80LBG-20GG/AG/s-HAp composite showed the noted porosity (81%; the measurement by micro-CT), absorption of simulated body fluid (1426%), adhesive strength (28.1 N) and hemostat time (7.5 h; the measurement by using simulated blood). The composite is also expected to assist the osteogenesis with its s-HAp.

Overall, the composite of s-HAp and natural plant-derived polymer seems to be a promising material for the bone hemostasis and regeneration.

Image

Recent Publications

- Tsukuda S, Umeda T, Koda S, Itatani K (2011) Fabrication of Flexible Porous Calcium-Deficient Apatite-Alginate Composite and Its Evaluation. IOP Conf. Ser. Mater. Sci. Eng. 18 192 192022.

- Shimizu A, Umeda T, Isogai A, Saito T, Koda S and Itatani (2011) Fabrication of Novel Film Containing Hydroxyapatite Nanoparticles/Cellulose Derivative and its Evaluation. IOP Conf. Ser. Mater. Sci. Eng. 18 192 192020.

- Mimura T, Umeda T, Musha Y and Itatani K (2013) Properties of novel bone hemostat prepared using hydroxyapatite, phosphoryl oligosaccharides of calcium and thermoplastic resin. J. Ceram. Soc. Japan. 121 68-73.

- Shima E, Umeda T, Musha Y and Itatani K (2016) Properties of novel bone hemostat by random co-polymer of ethylene oxide and propylene oxide with sugar-containing hydroxyapatite. Adv. Mater. Lett. 7 90-94.

- Suzuki N, Umeda T, Sumi T, Horikoshi S, Kuwahara H, Toyama T, Musha Y and Itatani K (2016) Rapid formation of hydroxyapataite layer on polyethertherketone by vacuum ultraviolet irradiation and microwave heating techniques. J. Ceram. Soc. Japan. 124 49-54.

Yeonjeong Noh is a student of Sophia graduate school. Her research interest is the fabrication of bone hemostasis and bone regenerate properties with natural plant-derived polymer fabricated with hydroxyapatite.

Email: ejelion@naver.com