Anticorrosive performance of the scratched coating systems on carbon steel in marine environment by electrochemical technique

1Hongling Li*, 1Xia Zhao, 1Baorong Hou

1 Institute of Oceanology, Chinese Academy of Science, Qingdao, 266071, China

Abstract

In practice engineering, defects were inevitable for protective coating systems on steel surface. In this paper, a composite coating system, including primer, middle coat as well as top coat, were used to protect the carbon steel against corrosion in marine environment. Among them, two environmental additives, glass fibers and thiourea were applied in middle coat to modify the coating system. The long-term corrosion durability and the self-healing ability of the scratched coating system were evaluated by multiple methods. Results of electrochemical technologies indicated that the coating system containing 0.5 wt.% fibers and 0.5 wt.% thiourea presented a good performance of corrosion protection and self-healing for carbon steel as immersing in 3.5% NaCl for 120d. The evolution of localized corrosion factor with time obtained from current distribution showed that fibers combined with thiourea could effectively inhibit the occurrence of the local corrosion for the scratched coating systems and greatly delay the development of corrosion process. Surface characterization suggested that adequate of thiourea could be uniformly absorbed on fibers for a long time to play an important role in protecting the carbon steel. At last, the schematic models were established to demonstrate the action of fibers and thiourea on the exposed surface of the carbon steel and the scratched coating system in the whole deterioration process.

Illustrated diagram of the role of thiourea for protection of  coating system

Biography

Hongling Li is a researcher on anticorrosion performance of organic coatings for about 15 years. She has done her research at the Institute of Oceanology of Chinese Academic of Science. She has attended seven conferences presenting her research works and has published thirty papers in high impact journals.