Fabrication of Micro/Nano- crystals of organic Dirac fermion system: Nano-scale electrocrystallization

Takako Konoike, Doctor of Sci. PhD, WPI-MANA, National Institute for Materials Science (NIMS), JAPAN

Abstract (300 word limit)

Statement of the Problem: Since the discovery of graphene, it attracted a great interest because the electrons in graphene behave like massless Dirac fermions. It shows anomalous behaviors resulting from the peculiar liner dispersion. It has been recognized that Dirac fermion system is also realized in organic conductorα-(BEDT-TTF)2I3 under high pressure [1]. This system is composed of organic molecule BEDT-TTF and inorganic anions I3. These molecules are stacked alternatively and forming a multi-layered structure of conducting and insulating layer, respectively. By taking advantage of its bulk nature, we have experimentally studied the physical properties of Dirac fermions in this compound [2-4]. In high magnetic field, the characteristic edge state with spin current at the sample edges is theoretically predicted. By using the micro/nano-crystals, which contains large amount of “edges”, we aimed to observe the evidence of the edge state of this system. Methodology: Micro/nano-crystal growth of α-(BEDT-TTF)2I3 based on  Nano-scale electrocrystallization was carried out by using “Nano-Wire Fabrication Kit” (Iwata Glass Industrial Co., Ltd. [5]) The electrodes used in the crystal growth were made on a Silicon substrate with 300nm SiO2. Platinum electrode were deposited on a masked substrate, and 5m gap was made by photolithography (Fig. 1). The substrate was set into a saturated THF solution of above two molecules. DC current was applied between the electrodes at 20C in incubator during 24h. Findings: The typical crystal obtained by this method is shown in Fig. 2. The shape of the grown micro-crystal resembles with that grown by usual electrocrystallization. The surface of the crystal is almost flat and specularly reflected suggesting that the crystal is high purity. Conclusion: By using the Nano-scale electrocrystallization, we could obtain high purity micro-crystals. We will study this micro-crystal to detect the evidence of the edge state and spin current.

Image

Figure 1: Sillicon substrate with Platinum electrodes.

Figure 2: 3D Laser microscple image of one of micro-crystal.

100m

Recent Publications (minimum 5)

- S. Katayama et al., Katayama S, Kobayashi A, Suzumura Y (2006) Pressure-Induced Zero-Gap Semiconducting State in Organic Conductor α-(BEDT-TTF)2I3 Salt. J. Phys. Soc. Jpn. 75: 054705.

- Osada T, Uchida K, Konoike T (2011) Magnetotransport of Massless Dirac Fermions in Multilayer Organic Conductors Journal of Physics 334: 012049.

- Konoike T, Uchida K, Osada T (2012) Specific Heat of the Multilayered Massless Dirac Fermion System. J. Phys. Soc. Jpn. 81: 043601.

- Konoike T, Sato M, Uchida K, Osada T (2013) Anomalous Thermoelectric Transport and Giant Nernst Effect in Multilayered Massless Dirac Fermion System. J. Phys. Soc. Jpn. 82: 073601.

5.    Hasegawa H, Kubota T, Mashiko S (2003) Fabrication of molecular nanowire using an electrochemical method. Thin Solid Films 438-439: 352-355.

Biography (150 word limit)

Takako Konoike has expertise in evaluation and passion in improving the various measurements under pressure and crystal growth of organic conductors, especially organic Dirac fermion system α-(BEDT-TTF)2I3. We have measured the specific heat and thermopower of organic Dirac fermion system under high pressure. We have succeeded in obtaining the first experimental results of the specific heat of Dirac fermions, and observing the giant Nernst effect reflecting the intrinsic nature of the zero-mode Landau level, which is characteristic of the Dirac fermion system. From these results, we can conclude that the high-purity organic crystal can provide an ideal testing ground for experimental studies of Dirac fermions.

Email:KONOIKE.Takako@nims.go.jp

Notes/Comments: