# Effect of substrate temperature on structure and electrical properties of sputtered transparent conducting film of La-doped BaSnO3

Alok Tiwari, Ming-Show Wong

Material Science & Engineering Department, National Dong Hwa University,

Hualien, 97401, Taiwan

### Abstract

Lanthanum (La) doped Barium Tin Oxide (BaSnO3) film is an excellent alternative for expensive Transparent Conducting Oxides (TCOs) film such as Indium Tin Oxide (ITO). However single crystal film of La doped BaSnO3 has been reported with a good amount of conductivity and transparency but in order to improve its reachability, it is important to grow doped BSO3 films on inexpensive substrate. La doped BaSnO3 thin films have been grown on quartz substrate by Radio Frequency (RF) sputtering at different substrate temperature (from 200oC to 750oC). The thickness of the film measured were varying from 360nm to 380nm with varying substrate temperature. Structure, optical and electrical properties have been studied. Carrier concentration seen to be decreasing as we enhance the substrate temperature while mobility found to be increasing up to 9.3 cm2/V-S. At low substrate temperature resistivity found was lower (< 3x10-3 ohm-cm) while sudden enhancement was seen as substrate temperature raises and trend continues further with increasing substrate temperature. Optical transmittance is getting better with higher substrate temperature from 70% at 200o C to >80% at 750oC.Overall, understanding of changes in microstructure, electrical and optical properties of thin film by varying substrate temperature have been reported successfully.

Recent Publications

[1] M.G. Smith, J.B. Goodenough, A. Manthiram, R.D. Taylor, W. Peng, W Kimball., J Solid State Chem. 98 (1992) 181..

[2] F.Q. Adurodija, H. Izumi, T. Ishihara, J. Mater. Sci. Mater. Electron. 12, 57 (2000

[3] Q. Lin, Y. Guo, T. Sun, C. Guo, D. Carnahan, M. Giersig, Y.Wang, J. Gao, Z. Ren, K. Kempa, Adv. Mater. 26, 873 (2014)

[4] Wu, M., Yu, S., He, L., & Yang, L. (2016).. Journal of Materials Science: Materials in Electronics, 27(12), 12604-12609.

[5] Y.G. Cai, W. Liu, Q. He, Y. Zhang, T. Yu, Y. Sun, Appl. Surf. Sci. 256 (2010) 1694.

Biography

I am very much interested to study the Multiferroics, correlations between structural, magnetic and transport properties of transition metal oxides applicable for energy storage devices. During my study and research work in the SONT, RGPV Bhopal, I have developed a wide range of skills to investigate the compositionstructure- properties relationships of geometrically frustrated oxide materials shows multiferroic properties. My strengths are synthesis of transitional metal oxides using solid state reaction, hydrothermal, monomode micowave method and films by using Pulsed Laser deposition and RF magnetron sputtering. Furthermore, I have hand on experience on various characterization systems such as powder XRD, SQUID (ac and dc), PPMS, SEM-EDX, UV-Vis, FT-IR. Apart from my experimental skills, I have published three  journal papers for my Work.

Email: aloktiwariiiser@gmail.com