Effect of epoxidized cardanol on poly(vinyl chloride)

as secondary plasticizer

Jie Chen, Ke Li

Institute of Chemical Industry of Forestry Products, Chinese Academy of Forestry, China

Abstract (300 word limit)

A epoxidized cardanol plasticizer derived from cardanol was synthesized and characterized by fourier transform infrared (FTIR), 1H -nuclear magnetic resonance (1H-NMR) and 13C -nuclear magnetic resonance (13C-NMR). Effects of the epoxidized cardanol used as secondary plasticizer for DOP in PVC blends were studied. Dynamic mechanical analysis (DMA),tensile test and thermogravimetric analysis (TGA) of PVC films plasticized with different content of epoxidized cardanol were investigated. The results indicated that the percent elongation increases with increasing epoxidized cardanol content. The epoxidized cardanol had better thermal stability than cardanol, the10% weight loss (T10) and 50% weight loss (T50) of which enhanced from 218.73 and 259.53 °C to 248.50 and 312.53 °C. And the plasticized films showed the thermal stability increased with increasing the content of epoxidized cardanol. When 8 phr DOP was replaced with epoxidized cardanol, the T10 and T50 increased by 9.58 °C and 5.53 °C respectively. The properties of volatility and extraction resistance of plasticizers were tested and showed similar or higher stability in those properties than that of DOP. Surface characterization of films by FTIR were also investigated.

Image

Recent Publications (minimum 5)

- Jie C, Ke L (2018) Synthesis of Tung-Oil-Based Triglycidyl Ester Plasticizer and Its Effects on Poly(vinyl chloride) Soft Films. ACS Sustainable Chemistry & Engineering 6: 642–651.

- Jie C (2018).Synthesis and application of a novel environmental C26 diglycidyl ester plasticizer based on castor oil for poly(vinyl chloride). Journal of Materials Science53: 8909-8920.

- Jie C, Ke L (2016). Synthesis and application of a novel environmental plasticizer based on cardanol for poly (vinyl chloride)[J]. Journal of the Taiwan Institute of Chemical Engineers 65: 488-497.

- Jie C (2016).Thermal behavior of epoxidized cardanol diethyl phosphate as novel renewable plasticizer for poly (vinyl chloride). Polymer Degradation and Stability 126: 58-64.

- Jie C (2015). A Novel Biobased Plasticizer of Epoxidized Cardanol Glycidyl Ether: Synthesis and Application in Soft Poly(vinyl chloride) Films. RSC Advances 5: 56171-56180.

- Jie C (2015). Synthesis and application of polyepoxide cardanol glycidyl ether as biobased polyepoxide reactive diluent for epoxy resin. ACS Sustainable Chemistry & Engineering 3: 1164-1171

Biography (150 word limit)

Jie Chen has completed his PhD at the age of 29 years from Beijing Forestry University. She has published more than 30 papers in reputed journals.

Email: chenjie_hi@126.com

Notes/Comments: