K4CaGe3O9:Mn2+,Yb3+: A Novel Orange-emitting Long Persistent Luminescence Phosphor With Special Nano Structure

Xufeng Zhou (PhD Student), Yuhua Wang*, Lanzhou University, China

Abstract (300 word limit)

A novel germanate based orange-emitting long persistent luminescence (PersL) phosphor: K4CaGe3O9(KCGO):Mn2+,Yb3+ has been successfully synthesized by the solid-state reaction. The special nano structures of KCGO:Mn2+ and KCGO:Mn2+,Yb3+ were indicated by transmission electron microscope (TEM) images that the block particles fo these samples are consist of many irregular spherical nano-particles and the size of these spherical particles is less than 10 nm. This special nano structure exist many defects and could provide precondition for the PersL properties of KCGO:Mn2+. Furthermore, after co-doped with Yb3+, the PersL properties have been effectively improved due to the new traps with high concentration caused by the nonequivalent substitution of Yb3+. With the optimum doping concentration and sufficient excitation with UV light, the afterglow of KCGO:0.02Mn2+,0.015Yb3+ can persist over 5 h above the recognizable intensity level (≧0.32 mcd/m2). Both fluorescence and phosphorescence spectra of KCGO:Mn2+,Yb3+ exhibit only one broad emission band, which belongs to the 4T1(G)-6A1(S) transitions of Mn2+. In addition, with the help of thermoluminescence (TL) curves, the processes and possible mechanism are studied and discussed.

Image

Recent Publications

- Xufeng Zhou, et al. (2018) Structure, bandgap, photoluminescence evolution and thermal stability improved of Sr replacement apatite phosphors Ca10-xSrx(PO4)6F2: Eu2+(x= 4, 6, 8). Dyes and Pigments, 152: 75-84.

- Xufeng Zhou, et al. (2018) K4CaGe3O9:Mn2+,Yb3+: A Novel Orange-emitting Long Persistent Luminescence Phosphor With Special Nano Structure. Journal of Materials Chemistry C, DOI: 10.1039/C8TC01845F.

Biography

Xufeng Zhou is a PHD student in Lanzhou University. His main research direction is solid luminescence material.

Email: 810773647@qq.com

Notes/Comments: