Facile Synthesis of Laminated Porous WS2/C Composite and Its Electrocatalysis for Oxygen Reduction Reaction

Huodi Huang, Xiaofeng Zhang, Shen Lin*

College of Chemistry and Materials Science, Fujian Normal University, Fuzhou, 350007, China

The Vulcan XC-72R supported WS2 nanocomposite (WS2/C）was prepared by solid reaction process combined with sonication. The as-prepared WS2/C nanocomposite presents a laminated porous structure by SEM and TEM characterization. The electrochemical experiments show that the onset potential and the limiting-current density of WS2/C is 0.78 V and 4.99 mA cm-2, respectively, which is much higher than that of WS2 (3.12 mA cm-2) and Vulcan XC-72R (2.79 mA cm-2). The number of transfer electrons in ORR at the WS2/C nanocomposite electrode is 3.70, which is close to four-electron process. Besides, the current density of WS2/C nanocomposites remained at 90% after 20000 s, indicating its superior electrochemical stability. All these facts reveal that the as-prepared WS2/C nanocomposite can be regarded as a promising cathode ORR catalyst for fuel cell.

Fig.2 ORR polarization curves of different modified electrode in 0.1 M KOH saturated with O2 at a rotating rate of 1600 rpm.

Fig.1 Cyclic voltammograms of WS2/C (A) and different modified electrodes(B) in 0.1 M KOH solution at Scan rate of 30 mV s-1.

Reference

[1] Yang Z, Nie H, Chen X, Chen X, Huang S. Recent progress in doped carbon nanomaterials as effective cathode catalysts for fuel cell oxygen reduction reaction. J Power Sources 2013; 236(16):238-249.

[2] Chua X J, Luxa J, Eng A Y S, Tan S M, Sofer Zd, Pumera M. Negative electrocatalytic effects of p-doping niobium and tantalum on MoS2 and WS2 for the hydrogen evolution reaction and oxygen reduction reaction. ACS Catal 2016; 6(9): 5724-5734.

[3] Chia X, Eng A Y S, Ambrosi A, Tan S M, Pumera M. Electrochemistry of nanostructured layered transition-metal dichalcogenides. Chem Rev 2015; 115(21): 11941-11966.

[4] Illathvalappil R, Unni S M, Kurungot S. Layer-separated MoS2 bearing reduced graphene oxide formed by an in situ intercalation-cum-anchoring route mediated by Co(OH)2 as a Pt-free electrocatalyst for oxygen reduction. Nanoscale 2015; 7(40):16729-36.

[5] Huodi Huang, Xiaofeng Zhang, Yi Zhang, Baohua Huang, Jiannan Cai and Shen Lin* Facile Synthesis of Laminated Porous WS2/C Composite and Its Electrocatalysis for Oxygen Reduction Reaction  Int J Hydrogen Energy 43(2018),8290-8297

Biography

Prof. Dr. Shen Lin obtained her B.S. Degree at Xia Men University in China in 1982, and completed her Ph.D. with Prof. Shixiong Liu at Fuzhou University in China in 2002. She works as a professor since 2000 in College of Chemistry and Material Science, Fujian Normal University, China. Her current research focuses on the development of new synthesis strategies of Pt/GNs based and non- noble metal electrocatalysts for their application in cathode and anode reaction of fuel cell, hydrogen evolution reaction and carbon dioxide reduction. Until now, she has published 20+ the related papers with average Impact Factor (corresponding author) over 3 (IF>3)

Email address: shenlin@fjnu.edu.cn

Notes/Comments: