Heat Treatment Characteristics of AM80-xMM(x=1, 3 , and 5 wt.%) Magnesium Alloy

Seoyeong Kim, Metallurgical and Materials Engineering, Gyeongsang National University, Republic of Korea

Ahruem Beck, Metallurgical and Materials Engineering, Gyeongsang National University, Republic of Korea

Sedong Lee, Metallurgical and Materials Engineering, Gyeongsang National University, Republic of Korea

Duckhyun Kim, Metallurgical and Materials Engineering, Gyeongsang National University, Republic of Korea

Sugun Lim, Metallurgical and Materials Engineering, Gyeongsang National University, Republic of Korea

Abstract (300 word limit)

The effects of misch metal addition on the microstructure, aging behavior and hardness of semi-solid Mg-7.5Al-0.3Mn-based alloys were investigated. In Mg-Al system alloys, the Mg17Al12 phase has a characteristic that the mechanical properties are rapidly lowered as the temperature is increased. In order to find solutions to these problems, the aging behavior and microstructural changes of AM80 alloy were investigated by adding 0, 1, 3, and 5 wt.% of misch metal. Misch metal is widely used to improve the high temperature properties of magnesium alloys at a relatively low cost. The composition of AM80 used in this experiment is shown in Table 1, and the composition of misch metal is shown in Table 2. The semi-solid alloys used for the experiments were prepared by cooling plate casting. The microstructural analysis on heat treatment and semi-solid casted alloys were carried out with the OM and SEM. And, its mechanical properties were evaluated by Vickers hardness. The microstructure of the as-cast alloys consists of a-Mg, Mg17Al12, phases formed by the addition of mish-metal, and the morphology of these intermetallic phases formed by the addition of misch metal shown a shape of a needle. In the case of the AM80 alloy without misch metal, the Mg17Al12 phase is distributed along the grain boundaries, and when misch metal is added, this element forms an intermetallic compound with Al to interfere with the formation of the Mg17Al12 phase. The inhibitory effect of misch metal formation of Mg17Al12 phase is also exhibited during heat treatment. When the misch metal is added, the precipitation amount of the Mg17Al12 phase decreases. As a result of measuring vickers hardness at room temperature, it was confirmed that the heat treatment efficiency is lowered as the amount of misch metal added increased.

Image

Recent Publications (minimum 5)

- Su Dong Park, Suk Bong Kang, Hyun Kee Cho (1999) Transformations: Effects of La, MM(Misch metal) Additions on Thermal Stability in High Mg Content Al-Mg Alloys. Korean Journal of Metals and Materials. Volume 37 (2), 163-169.

- A. Luo and A. Sachdev. (2010). Microstructure and Mechanical Properites of Magnesium-Aluminum-Manganese Cast Alloys. International Journal of metalcasting. 4, 51-59.

- Lim HK, Kim SK & Kim DH. (2012). J. Korea Foundry Society. Effect of Alloying Elements on Creep Behavior of Mg-Al Alloys, 31. 44-49.

- Park SH, Kim YM, Kim HS, Yim CD & You BS. (2012). Microstructure and Yield Asymmetry Behavior of Indirect-extruded Mg-Sn-Al-Zn Alloys, Transactions of Materials Processing. 21. 524.

- Kim DH. (2014). The Effect of Misch Metal(MM) Addition for Compression and Extrusion Behavior in Semi Solid AM80-xMM Magnesium Alloy. Gyeongsang National University

Su-Gun Lim, Prof. Dr. Eng

Main interests are;

Understanding the effects of microstructure, morphology and composition on the properties of light materials

Utilizing these knowledge to design improvement including Al- and Mg- base alloys, Development of high performance light materials via microstructure control

Email: suglim@gnu.ac.kr

Notes/Comments: