Title: XPS Analysis of Chemical Vapor Deposition Growth of Graphene from Ethanol

Name: R. Brajpuriya

Stanford University School of Medicine, CA 94305, USA

Recently, Carbon based nanomaterials have provided a new perspective in electronics owing to their very high charge carrier mobility and nanoscale dimensions. In particular, the carbon nanotubes and graphene have been shown to have promising performances suitable for high frequency electronic devices to efficient solar cells, flexible electronic displays to gas sensors, etc. However, the commercial exploitation of graphene is still a challenge because it is critical to synthesize large area graphene with high throughput and reliability. The key to solving this challenge requires us to develop synthesis and transfer methods to employ in the fabrication and transfer of large area single layer graphene films with an optimal degree of control. Considering low cost, scalability and high efficiency, we found chemical vapor deposition (CVD) method to be the most appropriate approach for producing graphene for large-scale manufacture. In this paper, therefore, our aim is to obtain improved and sustainable growth method of large area high-quality graphene. The cleanliness and the quality of the film are checked by x-ray photoelectron spectroscopy. D-parameter (19.5 eV) obtained from carbon Auger feature (C-KVV) and dominated single peak at 284.5 eV assigned to the sp2 graphitic C=C confirms the film deposited on Cu is graphene is clean with no contaminants.

Biography

Dr. Brajpuriya has more than 15 years of rich teaching and research experience including post doctoral research work in Italy, Germany and India. Presently, he is Director, Research & Pubication and Associate Professor of Nanotechnology. He was a visiting Scientist from Sept 2009 to June 2010 at Synchrotron Elettra, Trieste, and from Mar 2015 to August 2015, at ENEA, Rome, Italy. He has been awarded with numerous national and international. He is the member of many scientific and educational societies and referee for some of the reputed International Journals. He has published more than 75 research papers in International/National reputed journals. Dr. Brajpuriya research interest includes Carbon based Nanomaterials and Material Science.

Presenting author details 
Full name: DR. Ranjeet Kumar Brajpuriya		
Contact number:+918527769007
Twitter account:
Linked In account:

Session name/ number:
Category: (Oral presentation/ Poster presentation) Oral