Enhancement of thermoelectric properties in mechanically alloyed Bi0.4Sb1.6Te3 bulk nanocomposite containing Ti50Cu28Ni15Sn7 amorphous particles

Pee-Yew Lee, Institute of Materials Engineering, National Taiwan Ocean University, TAIWAN

Abstract (300 word limit)

During mechanical alloying of Bi, Sb and Te elemental powder mixture, the Bi0.4Sb1.6Te3 compound phase can be obtained after 2 hours of mechanical alloying treatment. The as-milled Bi0.4Sb1.6Te3 powders were further mixing with Ti50Cu28Ni15Sn7 amorphous particles to form Ti50Cu28Ni15Sn7 /Bi0.4Sb1.6Te3 composite powders after 30 minutes ball milling. The Ti50Cu28Ni15Sn7 / Bi0.4Sb1.6Te3 composite powders were consolidated into bulk samples with a diameter of 20 mm and thickness of 10mm by using vacuum hot pressing. The nano-/microstructured structure were observed for Ti50Cu28Ni15Sn7 /Bi0.4Sb1.6Te3 bulk samples. TEM bright-field image shows that the Ti50Cu28Ni15Sn7 amorphous phase with particle size of about 50 nm were homogeneously distributed along the grain boundary of Bi0.4Sb1.6Te3 matrix with grain size around 0.5~2.0 μm. The thermoelectric properties of Ti50Cu28Ni15Sn7/Bi0.4Sb1.6Te3 samples were measured. The results indicated, either use high purity (99.999%) or low purity (99.5%) Sb and Te as starting materials, the values of figure of merit (ZT) for the Ti50Cu28Ni15Sn7/Bi0.4Sb1.6Te3 bulk composite samples were found to increase with temperature in the range from 298 K to 580 K. It is the first time that such specific behavior has been observed. For 3 wt. % amorphous Ti50Cu28Ni15Sn7/Bi0.4Sb1.6Te3 specimen use high purity Sb and Te powders as starting materials, the maximum ZT value is only 0.9 at 473 K but is expected to reach 1.18 when the ZT curve is extends from 473K to 580K. For 1.75 wt. % amorphous Ti50Cu28Ni15Sn7/Bi0.4Sb1.6Te3 specimen fabricated from low purity Sb and Te powders, the maximum ZT value is 1.08 at 580 K, which is the highest ZT values among the existing typical low temperature thermoelectric materials has been measured at 580K.

Recent Publications (minimum 5)

- Lee Pee-Yew, Lin Pei-Ho (2018) Evolution of Thermoelectric Properties of Zn4Sb3 Prepared by Mechanical Alloying and Different     Consolidation Routes. Energies 11, 1200; doi:10.3390/en11051200.

- Lee Pee-Yew, Lin Yung-Sheng, Hu Chia-Jung, Hsu Chih-Feng (2017) The wear properties of Ti-based bulk metallic glass composites containing carbon particles. Journal of Alloys and Compounds 707:92.

Biography (150 word limit)

Prof. Pee-Yew Lee has completed his PhD at the age of 30 years from North Carolina State University. He joined the faculty at the National Taiwan Ocean University, as an associate professor of materials engineering in 1990 and was promoted to full professor in 1994.  From 1993 to 1999, He was director of institute of materials engineering at the National Taiwan Ocean University.  He has published more than 100 papers in reputed journals and serving as an editorial board member of Bulletin of Chinese Powder Metallurgy Association.

Email: pylee@ntou.edu.tw