# Influence of copper species on anti-biofouling and desalination performance of copper-modified thin-film composite reverse osmosis membranes

Andreina García*1, Yurieth Quintero1, Bárbara Rodriguez1, Rodrigo Quezada1-2, José Duguet2, Humberto Estay1

(1. Advanced Mining Technology Center (AMTC), University of Chile. 2. Centre of Biotechnology and Bioengineering (CeBiB), University of Chile)

### Abstract

The effect of the incorporation of copper nanoparticles (Cu and CuO) and Cu-(m-phenylenediamine) (Cu-mPD) oligomer complex into thin-film composite reverse osmosis (TFC-RO) membrane on their anti-biofouling and desalinization performance have been studied. Modified membranes by incorporating Cu and CuO nanoparticles during the interfacial polymerization process were obtained. Moreover, in situ formation of an (Cu-mPD) oligomer complex from copper chloride during the interfacial polymerization process was also successfully employed. Membranes were characterized by field emission scanning electron microscopy, Fourier transform infrared spectroscopy (FTIR), X-ray photoelectron spectroscopy (XPS), X-ray diffraction (XRD), atomic force microscopy, and contact angle measurements. Anti-biofouling properties were studied using a colony-forming unit (CFU) test in Escherichia coli as a model. Furthermore, an anti-adhesion test was developed using fluorescence microscopy. Membrane performance using a cross-flow cell was evaluated, and copper ion release test in long operation times were carried out. Characterization techniques allowed to confirm the formation of the polyamide active layer, the presence of incorporated copper nanoparticles and the in situ formation of the Cu-mPD oligomer complex. Modified membranes showed a slight decrease in hydrophilicity and higher surface roughness. However, an excellent anti-adhesion and bactericidal effect were observed in all cases, being more effective to Cu nanoparticles and (Cu-mPD) oligomer complex with respect to CuO nanoparticles. The anti-biofouling effect is attributed to the copper toxicity mainly due to the release of copper ions, whose release rates were higher in these two cases in comparison with CuO. Finally, the desalination performance of all modified membranes showed an important salt rejection (>98%) with stable water flux (about 30 L.m-2.h-1). In conclusion, the incorporation of copper into TFC-RO membranes during the interfacial polymerization process is a potential alternative method to improve the anti-biofouling capacities without impairing the performance of the membrane.

### Image

Recent Publications (minimum 5)

- N. Silva, S. Ramírez, I. Díaz, A. Garcia*, N. Hassan* (2019). Easy, Quick, and Reproducible Sonochemical Synthesis of CuO Nanoparticles. 12 (5): 804-808.

- M. Rosales, T. Zoltan, C. Yaradola, F. Gracia, A. García (2019). The influence of the morphology of 1D TiO2 nanostructures on photogeneration of reactive oxygen species and enhanced photocatalytic activity. Journal of Molecular Liquids 281:59-69.

- B. Rodríguez, D. Ozturk, M. Rosales, M. Flores, A. García* (2018). In situ formation of Cu-(m-phenylendiamine) oligomer complex within thin film composite reverse osmosis membranes (TFC-RO) for antibiofouling properties. Journal of Materials Science. https://doi.org/10.1007/s10853-018-2039-4.

- A. García*, B. Rodríguez, D. Ozturk, M. Rosales, D.I. Diaz, A. Mautner (2017). Incorporation of CuO nanoparticles into thin film composite reverse osmosis membranes (TFC-RO) for antibiofouling properties. Polymer Bulletin. 75 (5): 2053-2069.

- A. García*, Y. Quintero, N. Vicencio, B. Rodríguez, D. Ozturk, E. Mosquera (2016). Influence of TiO2 nanostructures on anti-adhesion and photoinduced bactericidal properties of thin film composite membranes.. RSC Advances. 6: 82941.

- A. García*, B. Rodríguez, D. Ozturk, M. Rosales, C. Paredes, F. Cuadra, S. Montserrat (2016). Desalination performance of antibiofouling reverse osmosis membranes. Modern Environmental Science and Engineering. 2 (7): 481-489.

Biography (150 word limit)

Andreina García is Chemical Engineer, Specialist in Natural Resources and Doctor in Chemistry. Currently, she is associated researcher of the Advanced Mining Technology Center, AMTC, University of Chile. Her research area is focused on the development of nano-technology for the treatment of polluted water and membranes for desalination process, in addition to the development of bio-technologies for the monitoring of heavy metals and water. Her experience is supported by international scientific publications, patents and in the management of projects of different kinds, from basic research, projects with the private sector, as well as R & D.

Email: andreina.garcia@amtc.cl.

Notes/Comments: