Abstract

MoS2 Nanosheets Covalently Functionalized with Pyrolytically Modified Polyacrylonitrile for Information Storage 
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The electrical conductivity of the laterally ordered polyacrylonitrile (PAN) can be improved by pyrolytic modification. Newly synthesized MoS2 nanosheets covalently grafted with PAN (MoS2-PAN) does not exhibit any electrical switching and memory effect in an ITO/MoS2-PAN/Au device under applied bias voltages. After annealing at 220°C for 4h, the resultant pyrolytically modified product “pyro-MoS2-PAN” shows good nonvolatile rewritable memory performance, with a large ON/OFF current ratio of 4  104 and lower switching on and off voltages of -1.09 and 1.24V. Highly reproducible memory I-V loops of more than 60 consecutive cycles have been achieved without clear degradation of the ON and OFF states. The first oxidation potential of pyro-MoS2-PAN is cathodically shifted over 530mV lower than that of MoS2-PAN, indicating the higher hole injection of pyro-MoS2-PAN when compared to MoS2-PAN. As expected, the non-annealed MoS2/PAN blends–based device does not show any memory effect under the same experimental condition. After annealing at 220°C for 4h, the blends exhibited unstable electrical switching and rewritable memory performance.
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