Abstract

MoS2 Nanosheets Covalently Functionalized with Pyrolytically Modified Polyacrylonitrile for Information Storage

- Bin Zhang, Fei Fan, Yaming Cao, Yu Chen*

Key Laboratory for Advanced Materials, Institute of Applied Chemistry, School of Chemistry and Molecular Engineering, East China University of Science and Technology, Shanghai 200237, China. Email: chentangyu@yahoo.com

The electrical conductivity of the laterally ordered polyacrylonitrile (PAN) can be improved by pyrolytic modification. Newly synthesized MoS2 nanosheets covalently grafted with PAN (MoS2-PAN) does not exhibit any electrical switching and memory effect in an ITO/MoS2-PAN/Au device under applied bias voltages. After annealing at 220°C for 4h, the resultant pyrolytically modified product “pyro-MoS2-PAN” shows good nonvolatile rewritable memory performance, with a large ON/OFF current ratio of 4  104 and lower switching on and off voltages of -1.09 and 1.24V. Highly reproducible memory I-V loops of more than 60 consecutive cycles have been achieved without clear degradation of the ON and OFF states. The first oxidation potential of pyro-MoS2-PAN is cathodically shifted over 530mV lower than that of MoS2-PAN, indicating the higher hole injection of pyro-MoS2-PAN when compared to MoS2-PAN. As expected, the non-annealed MoS2/PAN blends–based device does not show any memory effect under the same experimental condition. After annealing at 220°C for 4h, the blends exhibited unstable electrical switching and rewritable memory performance.

References

Y. Chen, B. Zhang, G. Liu, X. Zhuang, E.-T. Kang, Graphene and its derivatives: Switching ON and OFF，Chem. Soc. Rev. 2012, 41(13): 4688–4707

Y. Cao, X. Tian, J. Gu, B. Liu, B. Zhang, S. Song, F. Fan, Y. Chen, Covalent functionalization of black phosphorus with conjugated polymer for information storage, Angew. Chem. Int. Ed. 2018, 57:4543-4548

- F. Fan, B. Zhang, S. Song, B. Liu, Y. Chen, Pyrolytically modified polyacrylonitrile-covalently grafted MoS2 nanosheets for nonvolatile rewritable memory device, Adv. Electron. Mater. 2018, 4:1700397

- X.-D. Zhuang, Y. Chen, G. Liu, P.-P. Li, C.-X. Zhu, E.-T. Kang, K.-G. Neoh, B. Zhang, J.-H. Zhu,Y.-X. Li, Conjugated polymer functionalized graphene oxide: synthesis and nonvolatile rewritable memory effect, Adv. Mater. 2010, 22(15): 1731–1735

Biography for the corresponding author

Yu Chen is a full professor at East China University of Science and Technology. He received his Ph.D. in Organic Chemistry at Fudan University in July 1996. He has published more than 210 papers, reviews and communications in Chem. Soc. Rev., Prog. Mater. Sci., Nat. Commun., Angew. Chem. Int. Ed., J. Am. Chem. Soc., Adv. Mater., Adv. Funct. Mater., Mater. Horizons, Chem. Mater. and others.