# Cellulose acetate/Iron oxide nanocomposites: synthesis, characterization and environmental applications

Mónica A. Silva, M.T. Pessoa de Amorim,

2C2T, University of Minho, Campus de Azurém, Guimarães, PT

### Abstract (300 word limit)

### Statement of the Problem: In the last decades, the growing activity of the textile industries brings about some environmental problems, such as water pollution, which impose a sustainable development of the society and the world economy. To remediate the wastewater pollution there have been employed a number of efficient methods (adsorption, chemical and biological degradation, coagulation and membranes processes). Researchers have reported the membrane separation based on polymeric materials as one of the most promising technology3 for separation operations. However, some modifications are introduced into the membranes to make them more toughness, hydrophilic, and resistant to chemical/oxidizing attack.

The purpose of this scientific work is to describe the modification of the cellulose acetate film (CA) with a hematite nanoparticles, Fe2O3, by using phase inversion technique, and characterize the produced films in terms of surface roughness, hydrophilicity, chemical composition, thermal stability and dye rejection capacity. The photocatalytic degradation studies of the hydrolyzed dye are underway due to the necessity in the recycling of the nanocomposites films, making these photocatalyic films more affordable.

Methodology: Firstly, different size of hematite nanoparticles (NPs) was synthesized by the chemical precipitation method using different titre of the salt solution. Then, to prepare the CA/Fe2O3 films, with ~1 wt.% of NPs, the NPs were blended with the CA solution, as shown in Table 1. The films were prepared via non-solvent induced phase separation (NIPS). The structure and some properties of the nanocomposite films were characterized. Finally, the nanocomposite films were tested in a photocatalytic membrane reactor to evaluate the photocatalytic efficiency for the degradation of a hydrolyzed dye.

Findings: The produced films have presented nanoparticles into the polymeric matrix which means some morphological changes in the porous structure of the polymer and an increasing in the hydrophilic behavior. The chemical structure made by FTIR analysis spectra was typical of the CA films. In addition, the thermal stability was increased. Within 5 hrs, >80% of dye desorbed and decomposes from composite membranes’ surface by the effect of UV light.

Conclusions: The nanoparticles are successfully incorporated in the CA matrix and the modified films produced by a wet phase inversion technique can be considered as an effective dye adsorbent/catalyst.

### Table 1

### Designation and formulation of the nanocomposites films with 1 wt.% of NPs

| ### Membrane code | ### Titre of iron salt (M) | ### CA (mg) | ### NPs (mg) | ### DMF (mL) |
| --- | --- | --- | --- | --- |
| ### M0 | ### 0.0 | ### 1.5 | ### 0.0 | ### 8.5 |
| ### M1 | ### 0.05 | ### 1.45 | ### 0.5 | ### 8.5 |
| ### M2 | ### 0.1 | ### 1.45 | ### 0.5 | ### 8.5 |
| ### M3 | ### 0.2 | ### 1.45 | ### 0.5 | ### 8.5 |

Recent Publications

- Koszewska M (2018) Circular Economy — Challenges for the Textile and Clothing Industry. Autex Research Journal 18(4): 337–347.

- Rajasulochana P, Preethy V (2016) Comparison on efficiency of various techniques in treatment of waste and sewage water – A comprehensive review. Resource-Efficient Technologies 2(4):175-184.

- Ulbricht M (2006) Advanced functional polymer membranes. Polymer 47(7):2217-2262.

- Silva MA, Hilliou L, Pessoa de Amorim MT (2019) Fabrication of pristine‑multiwalled carbon nanotubes/cellulose acetate composites for removal of methylene blue. Polym Bull. https://doi.org/10.1007/s00289-019-02769-0

- Zahid M, Rashid A, Akram S, Rehan ZA, Razzaq W (2018) A Comprehensive Review on Polymeric Nano-Composite Membranes for Water Treatment. Journal of Membrane Science and Technology 8:1-20.

Mónica A. Silva has her expertise in photocatalysis and macromolecular synthesis. In the past 2 years, she has been working at 2C2T, University of Minho, Guimarães, Portugal (PT), in polymeric membranes optimization processing by doing their modification with nanoparticles (carbon nanotubes, TiO2 and Fe2O3). These composite membranes are used in dye rejection from wastewater effluents. The work permitted her the participation in three international conferences and the publication of two papers in recognized peer reviewed journals. Meanwhile, new applications of the membranes in the area of Biomedical Engineering are being doing by her.

Email: mabsilva2013@gmail.com

Notes/Comments:

This work was financed by PROJECT TSSiPRO  TECHNOLOGIES FOR SUSTAINABLE AND SMART INNOVATIVE PRODUCTS, NORTE-01-0145-FEDER-000015, and by national funds through FCTPortuguese Foundation for Science and Technology within the scope of the PROJECT UID/CTM/00264/2019.