PRECIPITATION-STRENGTHENED AND MICROLAYERED BULK COPPER- AND MOLYBDENUM-BASED NANOCRYSTALLINE MATERIALS PRODUCED BY HIGH-SPEED ELECTRON-BEAM EVAPORATION–CONDENSATION IN VACUUM:  STRUCTURE AND PHASE COMPOSITION

N. I. Grechanyuk, V. G. Grechanyuk, “Eletechmash” Ukraine A. Manulyk “Synergy ANTECH Services Corp.” Canada

The phase composition and structuration of three types of copper and molybdenum composite materials, 0.8 to 5 mm thick, which were condensed from the vapor phase at substrate temperatures 700 0C and 900 0C, are considered: precipitation-strengthened composites, micro-layered composites with alternating copper and molybdenum layers 1 to 10 mm thick, and bulk nanocrystalline composites with alternating layers thinner than 0.5 mm. Standard precipitation-strengthened Cu- and Mo-based materials condensed from the vapor phase at substrate temperatures 700–900  C can be produced over a relatively narrow composition range of the strengthening phase (0.1–3 wt.% Mo). When Mo content is 3–5 wt.%, the molybdenum particles change their shape from round to acicular and become discontinuous chains oriented perpendicularly to the vapor flow. If there is more than 5 wt.% of the second phase, the condensed composite materials (CCMs) show a layered structure. The layered structure can be observed in other CCM types (Cu–W, Cu–Cr, NiCrAlTi– Al2O3). Layered copper and molybdenum CCMs, 6 mm thick, produced on a rotating substrate heated to 700 ± 30 °C have been experimentally confirmed to belong to bulk nanocrystalline materials.  Keywords: rapid evaporation-condensation, copper, molybdenum, vacuum, precipitation-strengthened materials, layered materials, bulk materials.

Fig.1. Structure of CuMoZrCY bulk multi-layer composite

Recent Publications:

- A. Manulyk, S. Bhaduri  2018. Nano-composite Materials, Materials and Technology design for glass industry refractory materials”.  USA patent US9,856,163B2 Nano-composite Materials,  Materials and Technology design for glass industry refractory materials.

- A. Manulyk  2016. Oxidation resistance mechanism of TiAlSiCN and TiCrSiCN compositions made by plasma spark sintering at 1200°C  International conference on high temperature ceramic matrix composites Toronto ON,  Proceedings  6 pages.

- A. Manulyk  2015. Max phases: Understanding of erosion, corrosion, and oxidation resistance properties in TiAlSiCN and TiCrSiCN compositions. XXIV Materials Research Congress in Cancun Mexico, Proceedings 7 pages

- A. Manulyk , V. Shapovalov, Y. Nikitenko, D. Kovalshyk 2015. Production of amorphous alloys by special electrometallurgy methods. 27-th Canadian materials Science conference Halifax, Canada, Proceedings 6 pages.

- A. Manulyk, V. Shapovalov, V. Yuakusha, D. Kovalchyk 2015. Large refractory metals single crystals grown by plasma induction zone melting.  27-th Canadian materials Science conference. Halifax Canada. Proceedings 5 pages.

- A. Manulyk, K.Mishalenkov, 2013. Structure and composition of metallic ceramic coatings and their influence on the coating performance made by cold spray process MS&T 2013 Conference and Exposition Montreal, Canada. Proceedings 8, pages.

Biography

As a Materials Science professional, I have over 30 years of wide-ranging experience in welding, heat treatment, melting, coating, composites, process metallurgy, plasma metallurgy, electron-beam, and lasers technologies. My 20 publications, Certificates of invention and patents, numerous conference presentations demonstrate my success and accomplishments during these years.

Originally my professional career had started in one of the world-famous Research Centers - Electric Welding Institute named after E.O. Paton - Kyiv (Ukraine) upon my graduation from "The National Technical University of Ukraine" (department of Special Electric Metallurgy) in 1984.

I had also graduated "Kyiv's State University" (named after T.G. Shevchenko) in 1991, department of Physics of Materials & High-Temperature Super Conductivity, as well as finished Post-graduation courses in Electric Welding Institute (department of Plasma Metallurgy ) "Melting and Casting of Refractory Metals and Alloys."

I am a Professional Engineer in Ontario and have a master's degree in Metallurgy/Materials Sciences based on the evaluation done by this organization. I am also a licensed Chartered Engineer of IMMM (Mining, Material, and Metallurgy Institute) in the UK.  I am a Canadian citizen.

I also have extensive knowledge of technological processes and equipment:

- Electron-beam technologies, both: melting and evaporation;

- High-temperature plasma generators for coating and melting;

- PVD and CVD processes along with vacuum equipment;

- Infrared temperature measurable units,

- Magnetron sputtering process, machines, and induction furnaces;

- Spark Plasma Sintering technology;

- As well as different lab equipment (ESM, EDX, EBSD, TGA, and others).

Email: alex71021916@outlook.com