Paste your Logo here

Paste your Photograph Here

Title: Optical Properties of Nanocomposites

Name: Dondi dall’Orologio Giovanni

University of Bologna School of Dentistry, BO 40125, ITALY

In traditional composites, micron sized particles or agglomerates typically cause significant light scattering, hampering natural restorations; in nanocomposites the particle dimensions are small enough to produce highly translucent fillings. Color, Spectral Reflectance (R%), Scattering (S), Absorption (K), Translucency parameters(TP), Transmittance (T%) were calculated for Translucent (Trans), Enamel (E), Dentin (D) shades of a nanocomposite. The relative spectral radiance of each sample was measured against white and black ceramic tile backgrounds using a spectroradiometer. Specimens were measured inside of a color-assessment cabinet under constant D65 CIE standard illumination, illuminating/measuring configuration corresponded to CIE d/0°. Color coordinates in CIELAB color space: L*, a*, b* and the attributes of the color C* (chroma) and h° (hue angle) were calculated from the spectral reflectance data. S and K coefficients from Kubelka–Munk theory were calculated algebraically from the spectral reflectance data of each specimen. TP values were determined by calculating the color difference in CIELAB color space between readings against black and white backgrounds for the same specimen. Statistical analysis was performed using a one-way analysis of variance (ANOVA) and Tukey's multiple comparison test with Bonferroni correction. Trans shades showed the lowest mean R%, S and K values and the highest mean TP and T% in comparison with E and D shades. Nanofillers enable an improvement in the material’s esthetic and optical properties. There is a significant increase for precision of shade characters with higher translucency, thus providing excellent finish and gloss retention to the restoration.

Biography

Giovanni Dondi dall’Orologio, doctor in Medicine at the University of Bologna in 1969, achieved the post graduated title of specialist in dentistry. He was Assistant Professor in 1973 and Associate Professor from 1983. Head of the Division of Conservative Dentistry from 1973 to 2014. Director of the Master in Clinical Dentistry with advanced technology from 2003 to 2014.                                                             He experimented new technology with a spectrophotometer: this led to the development of a new machine for reading the color of composite restorations in vivo. He has published more than 75 papers in reputed international journals.

Presenting author details 
Full name: Giovanni Dondi dall’Orologio
Contact number: +39 3207175610 - +39 051377902

Email: giovanni.dondi@unibo.it
Session name/ number: Nanocomposites (day 2)
Category: Oral presentation