Title: Investigation of Pt-supported nanographene produced by in-liquid plasma for development of polymer electrolyte fuel cells

Name: Vladislav Gamaleev

Meijo University, Department of Electrical and Electronic Engineering,1-501 Shiogamaguchi, Tempaku, Nagoya 468-8502, Japan

Recently, various fuel cells, such as polymer electrolyte fuel cell (PEFC), are attracting a lot of attention owing to small size and at relatively low working temperature (below 80C), which makes possible usage of PEFCs in automobile and household power generation. However, PEFC has a problem with decrease of output caused by corrosion of amorphous carbon used as a catalytic carrier, which could be solved by use carbon nanostructures with stronger crystal structure than amorphous carbon. In this work, nanographene supported by Pt nanoparticles was synthesized and examined for possible application in development of PEFC with increased durability.

Nanographene was synthesized by in-liquid plasma generated in ethanol using AC high voltage (~11.7 kV). Amorphous component of synthesized nanographene was removed by hydrogen peroxide treatment and removal of amorphous carbon was confiremed by Raman spectroscopy. Platinum (Pt) nanoparticles were prepared on the surface of nanographene by the reduction of Pt salt precursors (H2Cl6Pt) in solution. Formation of Pt nanoparticles of diameter in range 2 - 4 nm was confiremed by transmission electron microscopy and X-ray diffraction measurement of Pt-supported nanographenes. Membrane electrode assembly (MEA) was constructed, where Pt-supported nanographene was used as the catalytic layer. Power generation characteristic of MEA were evaluated and current density for developed MEA was approximately 240 mA/cm2. From the electrochemical evaluation of Pt-supported nanographene, it was found that durability of Pt-supported nanographene was about seven times higher than that of carbon black, which looks promising for improvement of durability of PEFC.

Biography

Vladislav Gamaleev has completed his PhD at the age of 27 years from Kochi University of Technology, Japan. He is postdoctoral researcher of Meijo University. His research interests include generation of plasma at atmospheric and high pressure in gas and liquid phase, and plasma diagnostics by optical emission spectroscopy. Currently, he is focusing on the generation of oxygen radicals by atmospheric pressure plasma for biological and agriculture applications. Vladislav Gamaleev is a member of Japan Society of Applied Physics (JSAP).

Presenting author details 
Full name: Vladislav Gamaleev
Contact number: +81 (90) 4787-3587
Twitter account:
Linked In account: www.linkedin.com/in/gamaleev/

Session name/ number: Graphene & 2D materials

Category: Oral presentation