Optical and surface characteristics of direct composite, polished and glazed ceramic materials after exposure to tooth brush abrasion and staining solution

Firouzmandi M1, Miri M2

1 Associate professor, Department of Operative dentistry, oral and dental disease research center, Shiraz university of medical sciences

2 General Dentist, Private Practice

Aim and background: esthetic and structural reconstruction of anterior teeth may require application of different restoration material. In this regard combination direct composite veneer and ceramic crown is a common treatment option. Despite the initial matching their long term harmony in term of optical and surface characteristics is a matter of concern. The purpose of this study is to evaluate and compare optical and surface characteristic of direct composite, polished and glazed ceramic materials after exposure to tooth brush abrasion and staining solution.

Materials and Methods: ten 2 mm thick disk shape specimens were prepared from IPS empress direct composite and twenty specimens from IPS e.max CAD blocks. Composite specimens and ten of ceramic specimens were polished by using D&Z composite and ceramic polishing kit. The other ten specimens of ceramic were glazed with glazing liquid. Baseline measurement of roughness, CIElab coordinate and luminance were recorded. Then the specimens underwent thermocycling, tooth brushing and coffee staining. Afterword the final measurements were recorded. Color coordinate were used to calculate ΔE76, ΔE00, translucency parameter and contrast ratio. Data were analyzed by One-way ANOVA and post hoc LSD test.

Results: baseline and final roughness of the study group were not different. At baseline the order of roughness for the study group were as follows: composite < glazed ceramic < polished ceramic, but after aging no difference. Between ceramic groups was not detected. The comparison of baseline and final luminance was similar to roughness but in reverse order. Unlike differential

roughness which was comparable between the groups changes in luminance of glazed ceramic group was higher than other groups. ΔE76 and ΔE00 in composite group were 18.35 and 12.84, in glazed ceramic group were 1.3 and 0.79 and in polished ceramic were 1.26 and 0.85. These values for composite group were significantly different from ceramic groups. Translucency of composite at baseline was significantly higher than final, but there was no significant difference between these values in ceramic groups. Composite was more translucency than ceramic at baseline and final measurement.

Conclusion: Glazed ceramic surface was smoother than polished ceramic. Aging did not change the roughness. Optical properties (color and translucency) of composite were influenced by aging. Luminance of composite, glazed ceramic, and polished ceramic decreased after aging but the reduction in glazed ceramic was more pronounced.

Key words: ceramic, tooth-brush abrasion, staining solution, composite resin

Recent Publications (minimum 5)

- Fracture Strength and Marginal Adaptation of Conservative and Extended MOD Cavities Restored with Cention N.

Firouzmandi M, Alavi AA, Jafarpour D, Sadatsharifee S.

Int J Dent. 2021 Jul 6;2021:5599042. doi: 10.1155/2021/5599042. eCollection 2021.

- Antimicrobial Activity of Thermocycled Polymethyl Methacrylate Resin Reinforced with Titanium Dioxide and Copper Oxide Nanoparticles.

Giti R, Zomorodian K, Firouzmandi M, Zareshahrabadi Z, Rahmannasab S.

Int J Dent. 2021 Jan 30;2021:6690806. doi: 10.1155/2021/6690806. eCollection 2021.

- The effect of proanthocyanidin and casein phosphopeptide-amorphous calcium phosphate on the bond strength durability to caries-affected dentin.

Jowkar Z, Firouzmandi M, Tabibi S.

Clin Exp Dent Res. 2021 Jun;7(3):338-343. doi: 10.1002/cre2.368. Epub 2020 Dec 9.

- Marginal Fit of Full Contour Monolithic Zirconia in Different Thicknesses and Layered Zirconia Crowns.

Mohaghegh M, Firouzmandi M, Ansarifard E, Ramazani L.

J Int Soc Prev Community Dent. 2020 Sep 28;10(5):652-658. doi: 10.4103/jispcd.JISPCD_25_20. eCollection 2020 Sep-Oct.

- The effect of varying head tilt on the perceived color from composite resin and porcelain restorations: Simulating the effect of altering torque.

Sardarian A, Khaledi A, Firouzmandi M, Nematollahi H.

Am J Orthod Dentofacial Orthop. 2021 Jan;159(1):e35-e40. doi: 10.1016/j.ajodo.2020.08.013. Epub 2020 Nov 19.

- Effect of Simulated Pulpal Pressure on Knoop Hardness of Two Self-etch Adhesives with Different Aggressiveness.

Firouzmandi M, Shafiei F, Mohaghegh M, Hessami S.

J Contemp Dent Pract. 2020 Jun 1;21(6):673-677.

- Effect of silver diamine fluoride and proanthocyanidin on resistance of carious dentin to acid challenges.

Firouzmandi M, Vasei F, Giti R, Sadeghi H.

PLoS One. 2020 Sep 17;15(9):e0238590. doi: 10.1371/journal.pone.0238590. eCollection 2020.

- Effect of silver diamine fluoride on the bond durability of normal and carious dentin.

Firouzmandi M, Mohaghegh M, Jafarpisheh M.

J Clin Exp Dent. 2020 May 1;12(5):e468-e473. doi: 10.4317/jced.56303. eCollection 2020 May.

- Effect of Casein Phosphopeptide-Amorphous Calcium Phosphate on Fracture Resistance of Reattached Tooth Fragments Using Conventional and Self-Adhesive Bioactive Flowable Composite.

Firouzmandi M, Afzali N, Parsaie Z, Mohammadi N.

Eur J Dent. 2020 Mar;14(2):288-293. doi: 10.1055/s-0040-1710141. Epub 2020 Jun 5.

- Knoop Hardness of Self-Etch Adhesives Applied on Superficial and Deep Dentin.

Firouzmandi M, Khashaei S.

J Dent (Shiraz). 2020 Mar;21(1):42-47. doi: 10.30476/DENTJODS.2019.77805.0.

Maryam firouzmandi has her expertise in esthetic and restorative dentistry. She has attended at Operative dentistry department at Shiraz University of medical sciences since 2012. She is an active member of biomaterial research center and dental disease and diagnosis research center. She has been researching, teaching, and clinically practicing in her field of interest adhesive esthetic restorations for ten years.

Email: firouzmandim@gmail.com

Presenting author details 
Full name: Maryam Firouzmandi
Contact number: +98 912 601 6318
Session name/ number: Dental Research and Practice Management/ Restorative Dentistry and Endodontics
Category: Oral presentation