Hydrogenation of Biodiesel with Magnetic Platinum Catalysts

Falcão, Y. H. O. University of Brasília; Suarez, P. A. Z. University of Brasília; Jacinto, M. J.

# Abstract

Statement of the Problem: Recent changes in Brazilian fuel legislation increased the amount of biodiesel blended to diesel. Although the benefits of using biodiesel, there still some issues to be addressed, such as its low oxidative stability. The addition of antioxidants in fuels is not a permanent solution, since it only slows down the deterioration of the fuel. A promising alternative to the use of antioxidants is the selective hydrogenation of biodiesel. The goal of this work is to study the activity and selectivity of Platinum supported on a magnetic/silica core-shell nanoparticle as a catalyst for selective hydrogenation of Soybean biodiesel. Methodology: Pt@SiO2@Fe3O4 and Pt/Pd@SiO2@Fe3O4 were tested under different conditions in an autoclave reactor. Tests with BMI.BF4 and BMI.NTf2 as the reaction medium were also conducted. The ester content of the product was measured by the HPLC-UV method. The products were analyzed in order to determine the oxidative stability, viscosity, density and calorific characteristics. Results: Both catalysts showed no important selectivity on the hydrogenation of the methyl esters. Pt/Pd@SiO2@Fe3O4 had higher activity whilst the Pt@SiO2@Fe3O4 generated more selective products. The recycles of the catalysts were done, showing no changes in less than 3 reactions. In table 1 is shown the methyl esters contents for reactions with and without ionic solvents and the main results of the different analysis. Conclusions: Both catalysts are active for hydrogenation, with good results for formation of methyl oleate. Reactions with ionic solvent BMI.BF4 did not work and further analysis showed possible impregnation of the solvent on the catalyst. Reactions with BMI.NTf2 was noticed a selectivity for methyl oleate but with very reduced activity, demanding more time to achieve the aimed product.

# Table 1

Hydrogenation reactions methyl esters contents and their physical chemical analysis

|  |  | Blancb | Catalyst 1c | Catalyst 2d |
| --- | --- | --- | --- | --- |
| Methyl Esters Content | 18:3 cis | 7 | 3 | 1 |
|  | 18:2 cis | 52 | 49 | 6 |
|  | 18:2 trans | 0 | 0 | 1 |
|  | 18:1 cis | 26 | 31 | 12 |
|  | 18:1 trans | 0 | 0 | 40 |
|  | 18:0 | 7 | 9 | 32 |
|  | 16:0 | 8 | 8 | 8 |
| Physical Chemical Properties | Viscositye | 3.8 | 4.0 | 4.9 |
|  | Densityf | 863 | 860 | 852 |
|  | Melting Pointg | 0.53 | 4.84 | 25.3 |
|  | Oxidative Stabilityh | 10 | 95 | Beyond Limiti |

a Reactions conditions: 10 mL of biodiesel; 0.35%(w/w) of catalyst; 12,5 bar of H2 .; b Soybean Biodiesel; c Pt@SiO2@Fe3O4 ; d Pt/Pd@SiO2@Fe3O4 ; e mm2/s; f kg/m3 ; g °C; h Minutes; i More than 720 minutes.

Recent Publications

- CARVALHO, Myller S. et al. Chromatographic analyses of fatty acid methyl esters by HPLC-UV and GC-FID. J. Braz. Chem. Soc., [s.l.], v. 23, n. 4, p.763-769, abr. 2012. (SciELO).

- Carvalho, Myller S. et al. In situ generated palladium nanoparticles in imidazolium-based ionic liquids: a versatile medium for an efficient and selective partial biodiesel hydrogenation. Catalysis Science & Technology., p.480 - 488, 2011.

- SOUZA, Bruno S. et al. Selective partial biodiesel hydrogenation using highly active supported palladium nanoparticles in imidazolium-based ionic liquid. Applied Catalysis A: General, [s.l.], v. 433-434, p.109-114, ago. 2012. Elsevier BV

- JACINTO, M. J. et al. Platinum-supported mesoporous silica of facile recovery as a catalyst for hydrogenation of polyaromatic hydrocarbons under ultra-mild conditions. J Sol-gel Sci Technol, [s.l.], v. 77, n. 2, p.298-305, 2 set. 2015.

.