# Biomass combustion with CO2 capture by Chemical Looping

Alberto Abad, PhD

Francisco García Labiano, PhD

Teresa Mendiara, PhD

Luis F. de Diego, PhD

Antón Pérez-Astray, PhD student

María Teresa Izquierdo, PhD

Pilar Gayán, PhD

Juan Adánez, PhD

Instituto de Carboquímica (ICB-CSIC), Spain

### Abstract

Bioenergy and Carbon Capture and Storage (BECCS) is an interesting option to remove CO2 from the atmosphere, thus mitigating the CO2 emissions from the use of non-renewable sources, i.e. fossil fuels. BECCS has been identified as a relevant measure to achieve the target enforced by the United Nations Framework Convention on Climate Change (UNFCCC) in the Paris Agreement: to limit the increase in the average world temperature to 2 ºC above pre-industrial levels. However, implementing CO2 capture in bioenergy through common technologies has the drawback of high economic and energetic costs.

In this sense, the Chemical Looping Combustion (CLC) technology allows inherent CO2 capture at low cost during combustion. The benefits of CLC are based on avoiding the costly separation steps required in commercial CO2 capture processes, e.g. CO2 separation in flue gases or O2 production for oxy-fuel combustion, by the use of an oxygen carrier. The purpose of the oxygen carrier, usually a particulate metal oxide, is to transfer oxygen from air to fuel in order to avoid the direct contact between them. Thus, the oxygen carrier provides the oxygen required for combustion in the so-called fuel reactor. The oxygen carrier is later regenerated by air in the air reactor. The most common design of a CLC unit includes two fluidized bed reactors, being those mentioned fuel and air reactors, with the oxygen carrier continuously circulating among them. CLC has been widely investigated for the use of gaseous fuels and coal, but the interest of using biomass has recently increased considering that negative CO2 emissions would be possible.

The objective of this work is to contribute to the development of biomass combustion by CLC evaluating the use of new and highly reactive Mn-based materials as oxygen carriers. Experiments were performed in a continuous 500 Wth CLC unit at Instituto de Carboquimica (ICB-CSIC), consisting of two interconnected fluidized-bed reactors. After determination of both gas streams composition, the performance of the CLC process was assessed by calculating the CO2 capture rate and the combustion efficiency as a function of the operating conditions. During the experimental campaign, the temperature in fuel reactor and the circulation rate of the oxygen carrier were varied. In general, CO2 capture rates close to 100 % were obtained, which increased with temperature. In addition, high values of combustion efficiency were obtained. When the combustion was uncomplete, the major unburnt compounds from the fuel reactor were H2, CO and CH4. Likely, these unburnt gases could proceed from the volatile matter as a high conversion of char would be expected. Interestingly, the amount of tar detected was low, and they do not contribute significantly to the combustion efficiency.

Image

Recent Publications

- Mendiara T, Adánez-Rubio I, Gayán P, Abad A, de Diego LF, García-Labiano F, Adánez J (2016) Process comparison for biomass combustion: In situ Gasification - Chemical Looping Combustion (iG-CLC) versus Chemical Looping with Oxygen Uncoupling (CLOU). Energy Technology 4:1130-1136.

- Mei D, Mendiara T, Abad A, de Diego LF, García-Labiano F, Gayán P, Adánez J, Zhao H (2016) Manganese Minerals as Oxygen Carriers for Chemical Looping Combustion of Coal. Ind Eng Chem Res 55:6539-6546.

- Mei D, Mendiara T, Abad A, de Diego LF, García-Labiano F, Gayán P, Adánez J, Zhao H (2015) Evaluation of Manganese Minerals for Chemical Looping Combustion. Energy Fuels 29:6605-6615.

- Adánez-Rubio I, Abad A, Gayán P, de Diego LF, García-Labiano F, Adánez J (2014) Biomass combustion with CO2 capture by chemical looping with oxygen uncoupling (CLOU).Fuel Process Technol 124:104-114.

- Mendiara T, Abad A, de Diego LF, García-Labiano F, Gayán P, Adánez J (2013) Biomass combustion in a CLC system using an iron ore asan oxygen carrier. Int J Greenhouse Gas Control 19:322-330.

- Adánez J, Abad A et al (2012) Progress in chemical-looping combustion and reforming technologies. Progress in Energy & Combustion Science 38:215-282.

Biography

Alberto Abad is Tenured Scientist at the Instituto de Carboquímica at Zaragoza, belonging to the Spanish National Research Council (CSIC). His research has been always close linked to environmental challenges in energy production processes. Since 2002 he has been involved in the development of the Chemical Looping Combustion (CLC), one of the most promising technologies within the area of CO2 Capture and Storage (CCS) aiming to reduce global warming. More recently he has been actively engaged in the use of renewable fuels, such as biomass in Chemical Looping processes (bio-CLC) with the main objective to reach negative CO2 emissions in energy processes. He is author of more than 140 publications in international peer reviewed journals (h-index: 44) and 3 patents related to the development of oxygen carrier materials. He has been recognized as Highly Cited Researcher by Thomson Reuters within engineering area in years 2015 and 2016.

Email: abad@icb.csic.es

Notes/Comments: