# Enhancement of microbial fuel cell performance using nanomaterial decorated anode

Rehab H. Mahmoud,   PhD researcher, National research center, Egypt

### Abstract (300 word limit)

Microbial fuel cells (MFCs) have recently attracted significant interest owing to their unique ability to produce electricity from biodegradable organic matters. Microbial-electrode interactions, via microbial adherence and formation of electroactive biofilms, are essential to function the MFC. Therefore, anode materials and its structures play a crucial role in accelerating the formation of the biofilms.  In this work, a comparative study using different nano-structures has been made in order to enhance the maturation and cell viability with the biofilm matrix. Mutliwalled carbon nanotubes (MWCNTs), MWCNT/ MnO2 nanocomposite, reduced graphene oxide (RGO), RGO /Al2O3 mixture nanocomposite are the screened modifiers for boosting the biofilm formation. MWCNTs and RGO composites demonstrate high power densities   48.1 mW/m3, 24.5 mW/m3, respectively. Compared with CNT based anode, CNT/ MnO2 nano-composite achieved a much better electrochemical performance (power density 56.6 mW/m3and current density 377.3 mA/m2). This good performance can be ascribed to its high specific surface area and unique hierarchy architecture which facilitate fast electron and ion transport. Inspire of formation of the best well-defined matured anodic biofilm, RGO /Al2O3 nano MFC showed unexpected low power density (16.2 mW/m3).

The reported work provides a deep understanding of the interrelation between nanostructured based anodes and active microbial biofilm, suggesting future directions of those novel anode materials for MFC technologies.

.       Recent Publications (minimum 5)

- El-Baz F. K., Aly H. F., Ali G. H., Mahmoud R., Saad  S. A., (2016).  Antidiabetic efficacy of dunaliella salina extract in stz-induced diabetic rats. Int J Pharm Bio Sci, 7(3): (B) 465 – 473.

- Farouk K. El-Baz, Hanan F. Aly, Sayeda M. Abdo, Rehab Mahmoud, Safaa A. Saad., (2016). Dunaliella salina Alleviates Renal Dysfunction and Suppresses Inflammatory Cytokines in STZ-induced Diabetic Rats. Int. J. Pharm. Sci. Rev. Res., 38(2): 210-215.

- Rehab Mahmoud, Mohamed Ibrahim, Gamila Ali., (2016). Closed photobioreactor for microalgae biomass production under indoor growth conditions.  J. Algal Biomass Utln. 7 (1): 86-92.

- Hala S, Doma,  Sayeda M Abdo, Rehab H Mahmoud,  SA El Enin and G El Diwani., (2016). Production and characterization of biodiesel from microalgae cultivated in municipal wastewater treatment plant.  RJPBCS. 7(2): 1912-1919.

- Mona Hetta, Rehab Mahmoud, Waled El-Senousy, Mohamed Ibrahim, Gamila El-Taweel, Gamila Ali., (2014). Antiviral and antimicrobial activities of spirulina  platensis. Wjpps. 3(6): 31-39

Scheme 1. Selective enrichments of the electroactive biofilms

at nanostrucured anode surface

Rehab Hamdy is currently a Research assistant and PhD student in National research center, Egypt. and a member in Algal Innovation group, Center of Excellence for Advanced Sciences, Egypt (CEAS). Rehab is a 7 year experience in algae biomass cultivation in both close and open systems and bioenergy production. She works in many international projects for biomass, bioenergy and bioactive compounds production from microalgae. In 2016, Rehab attended 4th International advanced course "Microalgae Process Design-From Cells to photobioreactors". 8-15 July, 2016, Wageningen, Netherlands and in 2017, she got an internship to University College London, Cambridge University, Aston University, Birmingham to discuss some issues about (for designing, constructing and developing algae photobioreactors). Rehab PhD thesis is about bioelectricity production from bacteria and microalgae using Microbial fuel cell technology. Email: Rh.mahmoud@nrc.sci.eg