# ABSTRACT

Agricultural  wastes could  be  used  to  substitute wood fuel and charcoal. However, crop residues such as coffee or rice husks have low density resulting in high cost for handling, storage and transportation, and poor combustion behaviour. Biomass densification technology can be used to overcome these problems.   Knowledge   of  densification  conditions  and  thermochemical  properties of coffee husks is currently lacking, therefore limiting its use as a densified fuel. This  study  was  therefore  carried  out  with  the  aim  of  assessing  the  feasibility  of  producing densified fuel from loose coffee husks. In the study, composite samples of loose coffee husks were taken and analysed through proximate and ultimate analyses. Results of proximate and ultimate  analyses  were  used  for  evaluating  the  thermochemical  properties  of  coffee  husks. Based on the results of proximate and ultimate analyses, NOx  pollution  problem  since  the  Nitrogen  content  of  1.25%, 1.75% and 1.54% in SD, 25% CH:75%SD and 75% CH: 25% SD respectively exceeds  levels  for  biomass  fuels  recommended  by  European  Committee  for  Standardisation (CEN). The volatile matter content reported at 86.5% and 84% for SD and 25% CH:75%SD suggested that briquette prepared from SD and 25% CH:75% SD were easy to ignite and suitable for large-scale combustion and  gasification applications. The HHV of SD (19.34 MJ/kg ) and 25% CH: 75% SD (19.40 MJ/kg)  were  in the range of wood fuel and therefore they are competitive in terms of their heating values. In conclusion, briquette prepared from SD and  25% CH:75% SD have competitive heating  value, volatile matter and ash content for use  as a fuel  in  large-scale  combustion and  gasification application.  However, use of SD and  25% CH:75% SD briquettes produced at low die pressures could be hampered by its potential to produce excessive  NOx  pollutants.   For better production of briquettes from saw dust and combination with coffee husk, it is recommended to determine burning time and efficiency of the prepared briquettes.

Key Words: Briquettes, Proximate Analyses, Ultimate Analyses and Heating Value