# SiNW/GO  based Sensing Platform for VoCs of Infectious Diseases

Varsha Gautam, Amity University, PhD (Pursuing), Noida, India

### Abstract

Graphene Oxide (GO)

Transmission of infectious diseases is more rapid than their detections. We focused on this topic in view of the indispensable increase in mortality rate due to infectious diseases. So the only way to help us with better prevention and diagnosis is early identification. In this sense, we  emphasized on creating an electrochemical sensor model  based on the latest  Silicon nanowire (SiNW) derived technology for the detection of breath biomarkers also known as volatile organic compounds (VoCs) of infectious diseases. Coating of Graphene oxide (GO) is one of the efficient way to obtain improved physical and chemical properties for a sensor. Through electrochemical anodization and annealing treatment, GO coated silicon nanowire arrays were fabricated and their cyclohexane and formaldehyde sensing performance was investigated. The electrode formed was characterized using SEM,TEM,EDX,FTIR, XRD and Raman. In the due course of determining the sensitivity of VoCs towards various alkanes (cyclohexane), aldehydes (formaldehyde)  present in the exhaled  breath of patients with certain infections we found, SiNW/GO indicates the best response towards cyclohexane and formaldehyde. It showed the contrary response of + 1.03 and – 0.98 for 1ppm concentration of  cyclohexane and formaldehyde, respectively at room temperature. The limit of detection for the sensor was 1ppm. Response time of the sensor was 30 seconds and the sensor retrieved with the recovery time of 3 minutes and 2 minutes for cyclohexane and formaldehyde respectively. Therefore, with these outcomes, we hope that this sensor could pave the way for a novel strategy in the development of a  point of care breath analyzer for the detection of infectious diseases.

### Image

Silicon nanowires (SiNW)

Figure: Silicon nanowires decorated with graphene oxide (SiNW/GO) Sensor.

Recent Publications

- Bhattacharyya, D., Kumar, P., Mohanty, S., Smith, Y., & Misra, M. (2017). Detection of four distinct volatile indicators of colorectal cancer using functionalized titania nanotubular arrays. Sensors, 17(8), 1795.

- Song, L., Luo, L., Xi, Y., Song, J., Wang, Y., Yang, L., . . . Wang, F. J. N. r. l. (2019). Reduced Graphene Oxide-Coated Si Nanowires for Highly Sensitive and Selective Detection of Indoor Formaldehyde. 14(1), 97.

- Hermans, I., Nguyen, T. L., Jacobs, P. A., & Peeters, J. J. C. (2005). Autoxidation of cyclohexane: Conventional views challenged by theory and experiment. 6(4), 637-645.

- Obermeier, J., Trefz, P., Wex, K., Sabel, B., Schubert, J., & Miekisch, W. (2015). Electrochemical sensor system for breath analysis of aldehydes, CO and NO. Journal of breath research, 9(1), 016008.

- Yuvaraja, S., Kumar, V., Dhasmana, H., Kumar, A., Verma, A., & Jain, V. J. J. o. M. S. M. i. E. (2019). Ultraviolet detection properties of electrodeposited n-SnO 2 modified p-Si nanowires hetero-junction photodiode. 30(8), 7618-7628.

Biography

Varsha Gautam is pursuing Ph.D. in Biosensors from Amity University, India. Her research focus is "Biosensors for Infectious Disease Detection." She is currently working on making a breath analyzer to identify biomarkers that are found in the breath of different infectious disease. Her research interest includes Enzyme based sensors, Bio-nanotechnology, Bio- Biomedical diagnosis of diseases, Electrochemical sensors, VOC Sensors. Her expertise include- Synthesis of Advance Nanomaterials (Graphene oxide, silicon nanowire using metal assisted chemical etching techniques, gold nanoparticle). She has also published one paper in reputed journal.

Email: varshagautam2277@gmail.com

Notes/Comments