Exploring the relationship between thickness and the characteristic temperature of Mn1.56Co0.96Ni0.48O4±δ films

Wenwen Kong, PhD, Xinjiang Technical Institute of Physics & Chemistry of CAS, China

Abstract (300 word limit)

Mn1.56Co0.96Ni0.48O4±δ (MCN) thin films, a very special negative temperature coefficient (NTC) oxide material, have a best application prospects in detector and sensor fields. It exhibit the high temperature coefficient of resistance (TCR), the excellent aging resistance performance, the wide operating temperature range, the broad band optical response and the long stability in operation [1].The functional relationship correlating thickness (d) and characteristic temperature (T0) of the MCN films is formulated in this article. A series of MCN thin films with different thicknesses (d) are fabricated by Pulsed Laser Deposition process. The characteristic temperature (T0) values are 3675, 3352, 3087, 3366 and 3816 K for MCN films with thickness from 265 to 887 nm. We formulates the functional relationship correlating d and T0 of the MCN films by Lorenz analysis. It further demonstrates that a directly proportional relationship between the 1/T0 and can be certain. The present results will open a way to design a desired negative temperature coefficient thermistors by adjusting the thickness of films.

Image

Fig.1 the relationship between thickness and the characteristic temperature of Mn1.56Co0.96Ni0.48O4±δ films

Recent Publications (minimum 5)

- Kong WW, Wang JH, Yao JC, Chang AM (2018) PInfluence of oxygen atmosphere annealing on the thermal stability of Mn1.2Co1.5Ni0.3O4±δ ceramic films fabricated by RF magnetron sputtering. Ceramics International 44:1455-1460.

- Kong WW, Wei W, Gao B, Chang AM (2017) A study on the electrical properties of Mn-Co-Ni-O thin films grown by radio frequency magnetron sputtering with different thicknesses. Applied Surface Science. 423: 1012-1018.

- Kong WW, Wei W, Gao B, Chang AM (2016) Mn1.56Co0.96Ni0.48O4±δ flexible thin films fabricated by pulsed laser deposition for NTC applications. Materials Science and Engineering B. 206: 39-44.

- Kong WW, Gao B, Jiang CP, Chang AM (2015) Influence of the oxygen pressure on the preferred orientation and optical properties of the pulsed-laser deposited Mn1.56Co0.96Ni0.48O4±δ thin films. Journal of Alloys and Compounds. 650: 305-310.

- Kong WW, Chen L, Gao B, Zhang B, Zhao PJ, Ji G, Chang AM, Jiang CP (2014) Fabrication and properties of Mn1.56Co0.96Ni0.48O4 free-standing ultrathin chips. Ceramics International. 40: 8405-8409.

Biography (150 word limit)

Wenwen Kong has her expertise in temperature sensitive materials and components. The thesis is to study the structural, electrical and optical properties of negative temperature coefficient thin film thermistors or sensors by using PLD, RF sputtering and screen printing Method. The growth mechanism and conductive mechanism of preferred orientation, heteroepitaxial and flexible Mn-Co-Ni-O films has been studied before. Her resently results have opened a way to design a desired negative temperature coefficient thermistor by adjusting the thickness and period orientation of the ceramic films.

Email: kongww@ms.xjb.ac.cn