# Thermal shock resistance of segmented and porous Thermal Barrier Coatings applied by Atmospheric Plasma Spray

Andrés García, Jhonattan de la Roche, Alejandro Toro

Tribology and Surfaces Group

Natinal University of Colombia, Medellín

### Abstract

### Thermal Barrier Coatings (TBC) of Ceria and Yttria Stabilized Zirconia (CYSZ) were deposited using Atmospheric Plasma Spray (APS) technique obtaining conventional (porous) and Density Vertically Cracked (DVC) microstructures. Coatings were deposited over Inconel 625 and a NiCoCrAlY bond coat.  Four conditions of spraying were evaluated: one with the conventional porous microstructure obtaining a 15% of porosity, and three with DVC microstructures, in which three electrical current were used in the spraying process: 480A, 500A and 520A, obtaining crack densities of ~ 3, 3.7 and 3.3 cracks/mm respectively. An experimental procedure was carried out to assess the performance of the coatings to thermal shock resistance as follows: cycles of 5 minutes at 1020°C and quenching in water.  The change in crack density and porosity was evaluated in the coatings before and after failure.

### Keywords: DVC, APS, TBC, thermal shock, porous.

Biography (150 word limit)

Andrés García, mechanical engineering student at the National University of Colombia.

Email: anfgarciare@unal.edu.co

Jhonattan de la Roche, Msc. and PhD student at the National University of Colombia.

Alejandro Toro, PhD. Associated professor at the National University of Colombia and Tribology and Surfaces Group leader.