Investigation on microstructural characterization of
 TiB2-TiN composites

Yaghoub Pazhouhanfar a*, Abbas Sabahi Namini b,c, Saeid Sharifiyan Ghazijahani a, 
Hamidreza Sharifian Ghazijahani a, Seyed Ali Delbari d, Mehdi Shahedi Asl d

a Aliyazh Sanat Sahand Ipak Company, P.O. Box: 51576-13536, Tabriz, Iran

b Department of Engineering Sciences, Faculty of Advanced Technologies, University of Mohaghegh Ardabili, Namin, Iran

c Department of Engineering Sciences, Faculty of Advanced Technologies, Sabalan University of Advanced Technologies(SUAT), Namin, Iran

d Department of Mechanical Engineering, University of Mohaghegh Ardabili, Ardabil, Iran

* Corresponding authors: Y. Pazhouhanfar (Y-Pazhouhanfar@assico.ir)

Abstract

In this paper, the influence of titanium nitride as a sintering aid on the relative density and microstructure of TiB2 ceramic was examined. Monolithic TiB2 and TiB2 doped with 5 wt% TiN were sintered at 1900 ˚C for 7 min under the pressure of 40 MPa by spark plasma. The addition of TiN affected the microstructure of TiB2-based sample considerably depicting the finer grains in the as-sintered ceramic. Detail investigation by the map analysis and energy dispersive spectroscopy results revealed the formation of in-situ nano-sized hBN secondary phase in the TiN-doped TiB2. In addition, TiN played a remarkable role on increasing the relative density of TiN-doped TiB2 ceramic producing a nearly fully dense ceramic with relative density of 99.9% in comparison with the monolithic ceramic having 96.7% relative density.

Keywords: Densification; Microstructure; Spark plasma sintering; TiB2; TiN; hBN nano-platelets.