Evaluation of physical and mechanical characteristics of ZrB2–SiC-diamondnano composites

Saeid Sharifiyan Ghazijahani a*, Hamidreza Sharifian Ghazijahani a, Yaghoub Pazhouhanfar a, Abbas Sabahi Namini b,c, Seyed Ali Delbari d, Mehdi Shahedi Asl d

a Aliyazh Sanat Sahand Ipak Company, P.O. Box: 51576-13536, Tabriz, Iran

b Department of Engineering Sciences, Faculty of Advanced Technologies, University of Mohaghegh Ardabili, Namin, Iran

c Department of Engineering Sciences, Faculty of Advanced Technologies, Sabalan University of Advanced Technologies(SUAT), Namin, Iran

d Department of Mechanical Engineering, University of Mohaghegh Ardabili, Ardabil, Iran

* Corresponding authors: S. Sharifian Ghazijahani (saeedsharifiyan@gmail.com)

Abstract

The effect of adding various amounts of nano-diamond additive (0, 1, 2, and 3 wt%) on the densification behavior and mechanical properties of ZrB2-25 vol% SiC samples were investigated in this research. All samples were spark plasma sintered at 1900 °C under 40 MPa external pressure for 7 min. Relative density (RD) values higher than 99.9% were obtained for the samples with 0, 1, and 2 wt% nano-diamond, while adding 3 wt% diamond dropped the RD by ~1.2%. The XRD and microstructural evaluations revealed the formation of some in-situ phases, namely ZrC and B4C. The highest Vickers hardness (24.7 GPa) and fracture toughness (5.8 MPa.m1/2) were achieved for the samples doped with 2 and 3 wt% nano-diamond, respectively.

Keywords: ZrB2; SiC; nano-diamond; SPS.