Impacts of SiCw reinforcement on microstructure and mechanical characteristics of TiC-WCn matrix composites

Hamidreza Sharifian Ghazijahani a*, Saeid Sharifiyan Ghazijahani a, Yaghoub Pazhouhanfar a, Shahrzad Shaddel b,  Seyed Ali Delbari c, Mehdi Shahedi Asl c

a Aliyazh Sanat Sahand Ipak Company, P.O. Box: 51576-13536, Tabriz, Iran

b Department of Materials Engineering, Sahand University of Technology, Tabriz, Iran

c Department of Mechanical Engineering, University of Mohaghegh Ardabili, Ardabil, Iran

* Corresponding authors: H. Sharifian Ghazijahani (hamidsharifiyan1353@gmail.com)

Abstract

In this work, the influence of adding 0, 10, 20 and 30 vol% SiCw (silicon carbide whiskers) on the microstructure and mechanical properties of TiC-3 wt% WCn was investigated. All designed samples were spark plasma sintered under the same conditions: sintering temperature of 1900 °C, the external pressure of 40 MPa, and dwell time of 7 min. The sintered samples with 20 and 30 vol% SiCw reached the RD more than 100%. On the contrary, the lowest RD was related to the sample with 10 vol% SiCw. On the other hand, the most significant values of Vickers hardness (28.58 GPa) and flexural strength (694 MPa) were obtained for TiC-3 wt% WCn and TiC-3 wt% WCn-20 vol% SiCw composites, respectively. It was also discussed that the main reason for obtaining the RD>100% probably was due to the formation of nonstoichiometric TiCx over the SPS process.

Keywords: TiC, WC, SiC, Spark Plasma Sintering, Composite