# Comparative study for removal of cationic dye from aqueous solutions by manganese oxide and manganese oxide composite

Tooba Saeed, M.Phil. NCEPC, University of Peshawar, Pakistan

Abdul Naeem, Ph.D., NCEPC, University of Peshawar, Pakistan

### Abstract

Manganese oxide-poly vinyl chloride (MnO2-PVC) composite has been synthesized for the removal of methylene blue from aqueous solution. Manganese oxide (MnO2) was frst prepared by mixing manganese chloride tetra hydrated with tetramethylammonium hydroxide and hydrogen peroxide followed by functionalization with polyvinyl chloride (PVC). The successful synthesis of the composite was confrmed by Fourier transform infrared, X-ray difraction and energy-dispersive X-ray analysis. The point of zero charge and the surface area of MnO2 nanosheets were increased from 4.10 and 214 m2 /g to 5.01 and 226 m2 g, respectively, after functionalization with PVC. The adsorption experiments under diferent experimental conditions, such as pH, concentration, time, dosage and temperature, were conducted to study the removal of methylene blue (MB) from aqueous solution by MnO2 and MnO2-PVC composite. The adsorption capacity of MnO2-PVC was 16 times greater than pristine MnO2, which is attributed to its high surface area, stability, polarizability and porosity. The Langmuir isotherm model was a good choice to probe into the mechanism of adsorption. Moreover, the adsorption process followed the pseudo-second-order kinetics, and the intra-particle difusion was accompanied by the flm difusion for controlling the rate of adsorption. The thermodynamic parameters such as free energy, enthalpy and entropy indicated that the adsorption process was found to be exothermic and more spontaneous at 298 K. These results demonstrate that MnO2-PVC is an efcient, environment-friendly and versatile adsorbent for dyes removal from wastewater
Recent Publications

- Khan, A; Naeem, A and Mahmood, T. Thermodynamic study of adsorption of methyl orange and congo red from aqueous solutions by PVP-Functionalized ZnO., Russian Journal of Physical Chemistry, 94I, (2020) 1581-1586. DOI:10.1134/S0036024420080154.

- M.A. Alotaibi, I.Ud Din, A.I. Alharthi, P. Ahmad, A. Naeem, I.A. ElSayed, G. Centi, Synthesis, Characterization, and Magnetic Behavior of Cobalt-Ferrite Nanoparticles under Variant Temperature Conditions, Physics of the Solid State, (2020).

- Muhammad Anwar Sajad, Muhammad Saleem Khan, Saraj Bahadur, Abdul Naeem, Saneya Batool, Evaluation of chromium phytoremediation potential of some plant species of Dir Lower, Khyber Pakhtunkhwa, Pakistan, Acta Ecologica Sinica, 40 (2020) 158-165.

- Ihtisham Wali Khan, Abdul Naeem, Muhammad Farooq and Tooba Saeed, Reusable Na-SiO2@CeO2catalyst for efficient biodiesel production from non-edible wild olive oil as a new and potential feedstock, Energy Conversion & Management, 231 (2021) 113854. 170.

- Abdul Naeem, Ihtisham Wali Khan, Muhammad Farooq, Tahira Mahmood, Israf Ud Din, Zahid Ali Ghazi, Tooba Saeed, Kinetic and optimization study of sustainable biodiesel production from waste cooking oil using novel heterogeneous solid base catalyst, Bioresource Technology, 328 (2021) 124831. 71 Toob

Presenting author details 
Full name: Abdul Naeem
Contact number: 03329291972
Twitter account:
Linked In account:

Session name/ number: 
Category: Oral presentation