# Can Pulpal Floor Debonding be detected from Occlusal Surface Displacement in Composite Restorations?

João Batista Novaes Júnior, PhD, MDS, School of Dentistry - University of Minas Gerais, MG, Brazil.

### Abstract

### Polymerization shrinkage of resin composite restorations can cause debonding at the tooth-restoration interface. Theory based on the mechanics of materials predicts that debonding at the pulpal floor would half the shrinkage displacement at the occlusal surface. The aim of this study is to test this theory and to examine the possibility of detecting subsurface composite restoration debonding by measuring the superficial shrinkage displacements. A commercial dental composite with linear shrinkage strain of 0.8% was used to restore 2
groups of 5 models Class-II cavities (8-mm long, 4-mm wide and 4-mm deep) in aluminum blocks (8-mm thick, 10-mm wide and 14-mm tall). Group I had the restorations bonded to all cavity surfaces, while Group II had the restorations not bonded to the cavity floor to simulate debonding. One of the proximal surfaces of each specimen was sprayed with
fine carbon powder to allow surface displacement measurement by Digital Image Correlation. Images of the speckled surface were taken before and after cure for displacement calculation. The experiment was simulated using finite element analysis (FEA) for comparison. The Group I results showed a maximum occlusal displacement of 34.7±6.7µm and a center of contraction (COC) near the pulpal floor. Group II had a COC coinciding with the geometric center and
showed a maximum occlusal displacement of 17.4±3.8µm. The difference between the two groups was statistically significant (p-value = 0.0007). Very similar results were obtained by FEA. The theoretical shrinkage displacement was 44.8 and 22.4µm for Group I and II respectively. The lower experimental displacements were probably caused by slumping of the composite before cure and deformation of the adhesive layer. Clinical significance: The results confirmed that the occlusal shrinkage displacement of composite restoration was reduced significantly by pulpal floor debonding. Thus, the occlusal displacement of a composite restoration could be used to assess its interfacial integrity.

### Image

- b)

Fig.  Digital Image Correlation -calculated shrinkage displacement vectors (10 magnification) for (a) Group-I fully bonded restoration and (b) Group-II restoration debonded at the floor.

Recent Publications (minimum 5)

- Novaes, João Batista et al. Can pulpal floor debonding be detected from occlusal surface displacement in composite restorations? Dental Materials , Volume 34 , Issue 1 , 161 - 169

- Novaes, João Batista et al. Comparative Study of the Effect of Acid Etching on Enamel Surface Roughness between Pumiced and Non-pumiced Teeth. Journal of International Oral Health : JIOH. 2015;7(9):1-6.

- Novaes, João Batista et al. Residual Stresses and Cracking in Dental Restorations due to Resin Contraction Considering In-Depth Young's Modulus Variation, Applied Biological Engineering - Principles and Practice, Dr. Ganesh R. Naik (Ed.), ISBN: 978-953-51-0412-4, InTech, Available from: http://www.intechopen.com/books/appliedbiological-engineering-principles-and-practice/residual-stresses-and-cracking-in-dental-restorations-due-toresin-contraction-considering-in-depth

- Novaes, João Batista et al. Seven-year follow-up of esthetic alternative for the restoration of peg-shaped incisors: A case study of identical twins. General dentistry: 2008 vol 56, ed 01:74-7.

- Novaes, João Batista et al. Avulsion of permanent lower central incisors: esthetic-functional solution. Dental Traumatology, 24: 479–481.  doi:10.1111/j.1600-9657.2008.00630.x

Biography

João Batista Novaes Júnior has his expertise in Dentistry and Dental Materials. He had interest to discuss about the indication of different techniques to improving the quality and durability of restorations. He carried on  one research about restoration evaluation model  to verify the possibylity of detecting pulpal debonding from Occlusal Surface Displacement, using Digital Image Correlation evaluated images and Finite Elements Analysis. He completed his PhD in Dental Materials at the University of São Paulo, Brazil and postdoctoral studies at the Minnesota Dental Research Center for Biomaterials and Biomechanics (MDRCBB) - Minneapolis - University of Minnesota. He is Associate Professor of the Department of Clinical, Pathology and Surgery at the University of Minas Gerais, Belo Horizonte, Brazil.

Full Name: João Batista Novaes Júnior
Tel: +55 31 99947-6084
Session Name/Number
Category: (Email: novaes@ufmg.br