Title: Large Moments in bct FexCoyMnz ternary alloy thin films

Name: Yves Idzerda

Montana State University, Bozeman, MT  U.S.A.

Mn

Fe

Co

Establishing high magnetic moment materials in thin film form is critical for magnetic device applications.  Shown in the figure is the average magnetic moments of bct FexCoyMnz ternary alloy thin films deposited on MgO(001) determined from the X-ray magnetic circular dichroism measured elemental moments as a function of composition.  Thin film epitaxy stabilized the bct structure for 80% of the available ternary compositional space compared to only a 23% stability region for the bcc bulk phase.  A maximum average atomic moment of 3.2 B/atom was observed for a Fe0.32Co0.47Mn0.21 (well above the 2.4 B/atom found at the peak of the Slater-Pauling binary alloy curve). The compositions exhibiting high moments are not stable as a bcc structure in the bulk ternary phase diagram.

Biography

Yves Idzerda is currently the Department Head and Professor of Physics at Montana State University in beautiful Bozeman, MT.  He received his PhD in physics in 1987 from the University of Maryland. His current research interest is in characterizing and controlling nanostructured and ultra-thin film interface properties using novel characterization techniques that are element resolved and have strong interfacial sensitivity.

Presenting author details 
Full name: Prof. Yves Idzerda
Contact number:406-994-7838
Session name/ number:
Category: (Oral presentation)