The Superconducting behaviour in HgBa2Can-1CunO2n+2+δ for (n3)

Emad K. Al-SHAKARCHI, and Ali I. Al-JANABIi

Department of Physics, College of Science, Al-Nahrain University, Baghdad, Iraq e.mail: eks2000@hotmail.com

Abstract

Hg-based high-temperature superconductors (Hg-HTSs) have a similar structure to other superconducting cuprates [1]. The synthesis of HgBa2Can-1CunO2n+2+δ for (n4) was prepared using sealed evacuated quartz tube with Hg-free precursor Ba2CaCu2O5+δ and Ba2Ca2Cu3O7+δ obtained by solid state reaction. It was carried out to investigate the critical temperature, crystal structures and magnetic susceptibility. It was found that there were more enhancement in the peak intensities of the diffraction patterns, especially at (n=5,6) rather than the phase Hg-1223. The structure showed a tetragonal phase with (a=b=3.8297 Å) for (n=4) and nearly approach for another value of (n). While there is elongation in the c-axis for (n4), such that c=18.893 Å for n=4, c=22.134 Å for n=5, and c=25.33 Å for n=6. The resistivity measurements showed a decreasing in Tc-values as increasing in the Cu-layers in the structure, Tc=122, 103, 94 K, for n=4,5,6 respectively. The susceptibility measurements showed the presence of superconductivity and enhanced the resistivity behaviour for different value of (n)

Figure 1; the susceptibility behaviour for HgBa2Can-1CunO2n+2+δ (n=5)

Figure 2; the resistivity behaviour for HgBa2Can-1CunO2n+2+δ (n=5)

Recent Publication

1. S. H. Lafta, E. K. Al-Shakarchi, A. M. Musa, J. T. Svejda, D. Erni, J. Hippler, and M. Farle; Microwave Losses of Nanostructre Li-Ni Ferrites in X-band and Ku-band", Iraqi J. of Physics, 14(29), pp. 44-54, (2016).

2. E.K. Al-Shakarchi, S.H. Lafta, A.M. Musa, M. Farle, R. Salikov; Effect of Ni Content on Structural and Magnetic Properties of Li-Ni Ferrites Nanostructure Prepared by Hydrothermal Method",;  J Supercond Nov Magn, 29(4), (2016).

3. R.F. AL-Masoodi, and E.K. Al-Shakarchi; New High Temperature Superconductor Phase of Y-Ba-Cu-O System; IJARPS, 2(7), pp. 33-39, (2015).

4. A.I. Al-Janabi, and E.K. Al Shakarchi, Synthesis and Specification of Superconductor Compound Bi2Sr2Can−1 CunO2n+4+δ, J. Supercond Nov Magn, 28(1),(2015).

5. N.B. Mahmood, E.K. Al-Shakarchi, B. Elouadi, and X. Feaugas; Crystal Structure of BaxSr1−xTiO3 Fine Powder, J. of Modern Physics, 6, 70-77, (2015).

Biography

Dr. Emad K. Al-Shakerchi, professor in Solid State Physics/ Physics Department/ College of Science/ Al-Nahrain University/ Baghdad/ Iraq. He is Member of Nanotechnology Society/ Iraq. He has completed his PhD from Al-Nahrain University/ Baghdad/ Iraq. He is a member of the American Association for Science and Technology Society, USA. He is head of the research group in solid state physics at Al-Nahrain University/ College of Science/Physics department. He participated in a large number of international scientific meetings. He has published more than 35 papers in reputed journals and has been a member of the editorial board of JMP. He is interested in the experimental solid state physics, such as superconductor and magnetic materials, and ferroelectric materials. He supervised on M.Sc., and Ph.D. projects in different Iraqi universities, nearly 22 projects.

e.mail; eks2000hotmail.com