Luminescence characteristics and related damage evolution of carbon ion implanted GaN

# J.L. Liu a, L.X. Chen a, J.J. Wei a, L.F. Hei a, X. Zhang b, C.M. Li a*

a Institute for Advanced Materials and Technology, University of Science and Technology Beijing, Beijing 100083, P.R. China

b Institute of Low Energy Nuclear Physics, Beijing Normal University, Beijing Radiation center, Beijing 100875, P.R. China

Abstract: Carbon doped GaN has been widely studied and applied for p-type GaN and yellow light-emitting diodes. However, the sites carbon located, related with luminescence characteristics has not been confirmed. In this paper, GaN was implanted with carbon ion using dose of 1×1017cm-2 and 2×1017 cm-2 and energy of 30keV and 40keV. And then the implanted samples were annealed at 800℃ for 20min and 1h under the N2 atmosphere. The luminescence characteristics of carbon ion implanted GaN was evaluated by PL spectrum with wavelength of 325nm. The lattice damage of GaN was characterized by Raman spectrum and corresponding vacancy-defect evolution before and after annealing was measured by slow positron annihilation. The results showed that, most of carbon atoms would be located at the interstitial sites after carbon ion implantation due to the absorption of vacancies, and no obvious luminescence could be observed. As the implanted samples were annealed, strong yellow luminescence was emitted and the vacancy for N (VN) or vacancy for Ga (VGa) was reduced resulting from the migration of interstitial carbon (Ci) and formation of complex between them. By contrast, samples with higher dose showed stronger yellow light emission, which was related with the lower migration rate of Ci and saturated concentration of Ci-V complex.

Key word: GaN; carbon ion implantation; luminescence; slow positron annihilation; vacancy

Author, E-mail address:liujinlong111@163.com (J.L. Liu)

Corresponding author, E-mail address: chengmli@mater.ustb.edu.cn (C.M. Li)