# Heating effect in laser direct writing of Al and Cu particles on Si-Wafer substrate

Mohammad H. Azhdast, MSc, TU-Berlin, Germnay

Klaus D. Lang, PhD, IZM Fraunhofer Berlin, Germany

Hans J. Eichler, PhD, TU-Berlin, Germnay

Veronika Glaw, PhD, IZM Fraunhofer Berlin, Germany

Martin Kossatz, MSc, PacTech GMB, Nauen, Germany

### Abstract

Laser direct writing technique has an advanced micro-fabrication processes to pattern thin layers of conducting and insulating materials on substrates. The heating influence during the transferring process is presented by theoretical equations and experimental trials. Laser pulse energy and overlapping is considered for different test conditions. The Nd:YAG infra-red laser with 8 picosecond pulse duration has been used for the investigations. The copper and aluminium particles are evaporated in the vacuum chamber on the glass in the thickness of 500 nm. The Si-wafer substrates heated up to 300° during the Laser-induced forward transfer of the particles. The samples are annealed in the reflow oven and Electroless nickel is plated on the printed particles to have higher coalescence. The laser pulse energy and pulse overlapping varies throughout the process.

When the laser pulse duration is longer than the electron-phonon thermal relaxation time, the electrons and the lattice are at the same temperature since the absorbed laser energy transformed immediately into heat. The transferring process in the lower pulse durations is completely a thermal procedure and the pulse energy converted into heat immediately. By increasing the laser fluence above the printing threshold, wide areas around the deposited particles are seen because of the heat affected zone (HAZ). The peak surface temperature associated with a number of parameters as laser fluence, donor thickness and pulse width.

While using ultra short laser pulses, physical processes such as photochemical action plays and important role with thermal proceeding. Furthermore, It was derived that a thicker layer permits more heat rising and the temperature across is comparable to a very thin layer. The interface layer of a solid has a great importance in thermal motion, where the composition of the bulk material has been changed by particle movements.

Recent Publications

- M. H. Azhdast, M. Kossatz, H. J. Eichler, K. Lang, and V. Glaw, "Deposition of Al and Cu nanoparticles on Silicon Wafer using a Picosecond Nd:YAG Laser: An Experiment-based Parameter Optimization Guide," in Conference on Lasers and Electro-Optics, OSA Technical Digest, paper JTu5A.12.(2017)

- M. H. Azhdast, M. Kossatz, H. J. Eichler, K. Lang, and V. Glaw, "Comparison of nano particle implantation with picosecond lasers by concerning different wavelengths from Aluminum and Copper on Silicon wafer substrate" in Conference on Lasers and Electro-Optics, OSA Technical Digest, paper ATu4C.2. (2017)

- M. H. Azhdast, H. J. Eichler, K. D. Lang, and V. Glaw, “Adhesion mechanism between laser sputtered Aluminum nano particles on Si-Wafer by Nd:YAG laser, ” Conference on Lasers and Electro-Optics, OSA Technical Digest, paper ATh1K.7.(2016)

- M. H. Azhdast, O. Lux, H. Fritsche, H. J. Eichler, G. Azdasht, H. Lüdeke, V. Glaw, and K. Lang, "Laser Melting of Metal Powders Using Nd:yag and Compact Diode Laser for Micro Particle Deposition," inAdvanced Solid State Lasers, OSA Technical Digest, paper AM5A.2. (2015)

- M.H.Azhdast, “Arrangement for applying conductive nanoparticles onto a substrate,” Patent publication number: US20160346842 , SmartPac GmBH Technology Services, (2014)

Biography

Mohammad Hossein Azhdast has finished his two master degrees in Mechatroncs and Mechanical engineering and he is currently doing his PhD at Technical University of Berlin institute of Electrical engineering. . He has gathered some experiments in microelectronic devices, wire bonding, thin film production and laser application systems by working at PacTech GMBH. He has invented a new model after years of studies for laser implementation of nano seeds on the silicon wafer substrates in the liquid chamber. He has developed the high speed solder jetting machine which was presented in the CLEO-2017 conference. His research interests are: laser direct writing process for nano particle printing, Electroless metal plating, Solder bumps for interconnections and laser industrial applications in the Photovoltaic and solar cells.

Email: azhdast@physik.tu-berlin.de

Notes/Comments:

I would be grateful if I could have my chance to present my paper in 9th international conference on Optics, Photonics and lasers in July 2018 Berlin, Germany