Title: The application of polymeric composite nanoparticles for treating hepatic fibrosis via specific delivery of gallic acid to hepatic stellate cells

Shaimaa A.A. Radwan1, Walaa H. El-Maadawy*2, Carol Yousry2, Aliaa N. ElMeshad2, Raguia A. Shoukri2

1Department of Pharmaceutics and Industrial Pharmacy, Faculty of Pharmacy, Cairo University, Kasr Al Aini street, Cairo, PO Box 11562, Egypt.

2Department of Pharmacology, Theodor Bilharz Research Institute, Kornaish El Nile, Warrak El-Hadar, Imbaba (P.O. 30), Giza 12411, Egypt

E-mail: w.elmadawy@tbri.gov.eg

Gallic acid (GA), a polyphenolic compound, is reported to possess potent antifibrotic effects in experimental animals, but exhibits low bioavailability due to its rapid clearance. Accordingly, we designed polymeric composite nanoparticles (NPs) as specific targeted delivery system for GA into hepatic stellate cells (HSCs); pivotal cells in orchestrating hepatic fibrogenesis. GA-loaded-NPs were prepared by solvent evaporation technique and characterized by different techniques. Cytotoxicity of GA-loaded-NPs was evaluated in rat HSCs cell line and primary hepatocytes using sulforhodamine B (SRB) assay. We also recorded the uptake of GA-loaded-NPs and their effects on cell migration in activated HSCs. The gene expressions of collagen I (col-1α), transforming growth factor (TGF)-β1 and α-smooth muscle actin (α-SMA) in HSCs were measured using qRT-PCR. Thereafter, bio-distribution of GA-loaded-NPs in rats was monitored via confocal laser scanning microscopy (CLSM). Results revealed that GA-loaded-NPs showed mean Particle size= 230nm, zeta potential= -33mV, polydispersity index= 0.22, encapsulation efficiency= 66 %w/w and in vitro drug release profile with burst release in the first hours followed by a sustained GA release for 24 hours. GA-loaded-NPs were more cytotoxic on HSCs by 80% than free GA solution without showing any cytotoxic effects on hepatocytes. GA-loaded-NPs exhibited enhanced uptake in activated HSCs and inhibition of migration and fibrogenic genes expression of col-1α, TGF-β1and α-SMA in HSCs. Furthermore, CLSM illustrated higher accumulation of GA-loaded-NPs in liver than other organs. This is the first study that clearly shows the efficacy of GA-loaded NPs targeted delivery for HSC as a promising therapeutic approach for liver fibrosis.

Bibliography

Walaa El-Maadawy “Researcher at the Pharmacology Department, Theodor Bilharz Research Institute (TBRI)” has completed her PhD in 2017 from Faculty of Pharmaceutical Sciences, Cairo University in the field of Pharmacology &Toxicology. She is also the Moderator of the Research Ethics Committee, TBRI. Her research work focuses on: pharmacokinetics, bioavailability and bioequivalence studies; investigation of therapeutic approaches for hepatic fibrosis and fatty liver diseases. She has published seven research articles in reputed journals and participated in four research projects sponsored by international and national agencies.

Presenting author details 
Full name: Walaa Hamido El-Sayed El-Maadawy
Contact number: 002-01005712421
Category: Oral presentation