Role of p-element sublattice in magnetic ordering of ZrNiAl-type RMn{Si, Ge}0.33Ga0.67 and RMnGe0.5Ga0.5 (R = Tb and Dy) compounds

A. V. Morozkin a*, O. Isnard b,c, A.K. Nigam d, R. Nirmala d, S. Quezado e, S.K.Malik e

a Department of Chemistry, Moscow State University, Leninskie Gory, House 1, Building 3, Moscow, GSP-2, 119992, Russia

b CNRS, Insitut. Néel, 25 rue des Martyrs BP166 x F-38042 Grenoble, France

c Université Grenoble Alpes, Inst. Néel, F-38042 Grenoble, France

d Indian Institute of Technology Madras, Chennai 600 036, India

e Departamento de Física Teórica e Experimental, Universidade Federal do Rio Grande do Norte, Natal,59082-970, Brazil

*Corresponding author: A.V.Morozkin, E-mail: morozkin@tech.chem.msu.ru

    - Abstract

Specific features of p-element sublattice have been studied for ZrNiAl-type {Tb, Dy}MnGe0.33Ga0.67 and {Tb, Dy}MnGe0.5Ga0.5 compounds (space group P-62m, No.189) by magnetization and neutron diffraction experiments. {Tb, Dy}MnGe0.33Ga0.67 and {Tb, Dy}MnGe0.5Ga0.5 compounds exhibit antiferromagnetic ordering  in wide temperature interval with antiferromagnetic behaviour of field dependent magnetization at 5 K.

Neutron data obtained between ~250 K to 1.7 K in zero applied field show the evolution of magnetic structure of TbMnGe0.33Ga0.67: ab-plane square modulated antiferromagnet with K1 = [±1/3, ±1/3, 0] propagation vector from ~250 K to ~ 150 K, a square modulated abc-antiferromagnet with K1 = [±1/3, ±1/3, 0] and K2 = [±1/4, ±1/4, 0] vectors between ~150 K and ~96 K and a sine modulated abc-antiferromagnet with K1 = [±1/3, ±1/3, 0], K2 = [±1/4, ±1/4, 0] and K3 = [1/2, 1/2, 0] vectors below 96 K and down to 1.7 K.

Similar to TbMnGe0.33Ga0.67, the magnetic structure of TbMnGe0.5Ga0.5 is a sine modulated abc-antiferromagnet with K1 = [±0.3235(5), ±0.3235(5), 0] and K2 = [±1/4, ±1/4, 0] propagation vectors from 160 K to 120 K, whereas it exhibits sine modulated abc-antiferromagnetic ordering with K1 = [±0.3231(2), ±0.3231(2), 0], K2 = [±1/4, ±1/4, 0] and K3 = [1/2, 1/2, 0] vectors from 120 K to 2 K.

    - Image

Recent Publications

- A.V.Morozkin, New ZrNiAl-type RmnGe0,5Ga0,5 compounds (R = Sc, Y, Lu, Sm, Gd-Ho, Tm), J.Alloys Compd., 352 (2003) L1-L2. doi:10.1016/S0925-8388(02)01129-5.

A.V.Morozkin, New R3Mn3GaSi2 compounds (R = Tb-Tm, Lu), J.Alloys Compd., 363 (2004) L1-L2. doi:10.1016/S0925-8388(03)00466-3

A.V. Morozkin, R.Welter, T.I.Ivanova, M.V.Makarova and O.L.Makarova, Magnetic structure of the ZrNiAl-type Dy3Mn3SiGa2 compound, J.Alloys Compd., 415 (2006) 23-25.

A.V. Morozkin, R. Nirmala, J. Arout Chelvane, A.K. Nigam, Magnetic properties of ZrNiAl-type R3Mn3GeGa2 compounds (R = Y, Gd, Tb, Dy, Ho and Er), Journal of Alloys and Compounds 476 (2009) 33–42. doi:10.1016/j.jallcom.2008.09.145

A.V. Morozkin, Lindomar Carvalho, R. Nirmala, S.K. Malik, O. Isnard, Magnetic properties of ZrNiAl-type R3Mn3SiGa2 compounds (R = Y, Gd, Tb, Dy and Ho), Journal of Alloys and Compounds 502 (2010) 261–269. doi:10.1016/j.jallcom.2009.11.130

Biography

Since 1997 A.V.Morozkin work for rare earth intermetallic compounds: ternary 'Rare Earth – Transition metal – p-element' systems, crystal structure, magnetic structure and magnetic properties of rare earth compounds.

Email:morozkin@tech.chem.msu.ru