# Encapsulation and real life reproducibility of graphene devices

Abhay A. Sagade, PhD,

Department of Engineering, University of Cambridge, 9 JJ Thomson Avenue, Cambridge, CB3 0FA, UK

### Abstract (300 word limit)

As many graphene-based electronic and optoelectronic device concepts begin to make the transition from the research laboratory into real world applications it is imperative that factors such as long term stability and large area reproducibility are addressed. Graphene is inherently highly sensitive to environmental factors such as ambient air, lithography resists and polymers used in the transfer process which cause unintentional, generally p-type, doping and hysteretic [7–10] behavior in field effect devices. Many of the graphene field devices need ambipolarity [1]. To overcome these issues device encapsulation and passivation is required.  Atomic layer deposition (ALD) of oxides provide two-fold benefits. Firstly, Al2O3 act as a moisture barrier which add long term stability and protection of devices from humidity and other atmospheric effects. Secondly, the ALD process has been shown to effectively passivate charge trap sites such as silanol (SiOH-) groups at the SiO2—graphene interface which are responsible for much of the observed unintentional doping and hysteretic device behavior. We have developed two different routes to enhance the nucleation of ALD oxides on hydrophobic graphene surface. In first approach an ex-situ nucleation layer of 2 nm Al film was deposited with appropriate amount of oxygen control by e-beam evaporation [2]. While in second route an in-situ nucleation was created by pulsing water precursor in the ALD chamber [3-5]. In both the methods highly-air stable and reproducible GFETs are obtained. We have shown continuous hundreds of DC measurements in ambient which do not show any hysteresis and shifts of Dirac points with negligible doping concentration in graphene channel. It paves the way to speed up the production of graphene devices for real life applications.

### Image

Figure: ALD encapsulation employed by (a) ex-situ nucleation, (b) in-situ nucleation of GFETs. (c) A concept of fabricating multi-stacked graphene chip with high performance encapsulation.

Recent Publications (minimum 5)

- Dauber, J et al. (2015) Ultra-sensitive Hall-sensor based on graphene encapsulated in hexagonal boron nitride Appl. Phys. Lett. 106: 193501.

- Sagade, AA et al. (2015) Highly air stable passivation of graphene based field effect devices Nanoscale 7: 3558-3564.

- Van Veldhoven, ZA et al. (2016) Electronic properties of CVD graphene: The role of grain boundaries, atmospheric doping and encapsulation by ALD Physica Status Solidi DOI: 10.1002/pssb.201600255.

- Aria, AI et al. (2016) Parameter Space of Atomic Layer Deposition of Ultrathin Oxides on Graphene ACS Appl. Mater. Interfaces 8: 30564–30575.

5. Alexander-Webber, JA et al. (2016) 6) Encapsulation of graphene transistors and vertical device integration by interface engineering with atomic layer deposited oxide 2D Material 4: 011008.

Biography (150 word limit)

Dr. Sagade is a researcher in the Electrical Engineering Division of Department of Engineering at University of Cambridge. He is also associated with EPSRC Centre for Innovative Manufacturing in Large-Area Electronics focusing on the designing of novel electronic devices to be printed on flexible sheets and exploring the possibilities for high speed testing of large-area electronics produced by reel-to-reel (r2r) manufacturing. He has Ph. D. in Physics from Dr B. A. M. University, Maharashtra, India. Also he has worked at JNCASR Bangalore (DST Nano fellowship) and AMO GmbH Germany (part of Flagship Graphene Project). He has co-authored more than 35 peer-reviewed publications and 3 US patent applications. Dr. Sagade has developed graphene device encapsulation process which assist in persisting its novel properties in ambient for several months with negligible hysteresis in DC measurements which enables real life applications usage of graphene. Dr. Sagade is a member of AAAS and MRS-Singapore.

Email: aas73@cam.ac.uk, aas_phy@aol.in

Notes/Comments